Supplementary Information for: Formamidinium + Cesium Lead Triiodide Perovskites:  Discrepancies between Thin Film Optical Absorption and Solar Cell Efficiency

Biwas Subedi, Lei Guan, Yue Yu, Kiran Ghimire, Prakash Uprety, Yanfa Yan, and Nikolas J. Podraza

Department of Physics & Astronomy and Wright Center for Photovoltaics Innovation & Commercialization, University of Toledo, Toledo, OH  43606, USA

Optical Properties

Fig. S1 shows numerically inverted complex dielectric function (ε = ε1 + iε2) for the spectral range near the band gap for which the observed change in ε for varying Cs concentration is more pronounced. Tabulated form of numerically inverted ε is also provided here (Table S3). After the numerically inverted ε spectra are obtained for the full region, critical point (CP) analysis using the first derivative of ε2 spectra, dε2/dE is performed to identify CP positions more accurately. To discard the noise in low energy region, the model fit for dε2/dE spectra with experimental data is performed on the 1.2 – 5.89 eV photon energy

Fig. S1. Complex dielectric function (ε = ε1 + iε2) of FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite thin films in the near band gap region.

range using CPPB oscillators. The experimental and corresponding model fit dε2/dE spectra of FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite thin films are shown in Fig. S2. Table. 1 shows the fit parameters namely amplitude (An), broadening (Γn), CP energy positions (Ecn), and phase factor (θn) used to describe the dε2/dE spectra of FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite thin films.

Fig. S2. The experimental and corresponding model fit dε2/dE spectra of FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite thin films.

Table 1. Fit-parameters to describe the dε2/dE spectra of FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite thin films using CPPB oscillators.

- x = 0.0

| CPPB | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| An | 25 ± 3 | 23 ± 2 | 9.0 ± 1 | 12 ± 1 | 10 ± 1 | 11 ± 1 | 2 ± 1 | 4 ± 2 |
| n (eV) | 0.040 ± 0.004 | 0.08 ± 0.01 | 0.8 ± 0.1 | 0.2 ± 0.03 | 0.6 ± 0.1 | 0.9 ± 0.1 | 0.82 ± 0.6 | 1.0 ± 0.6 |
| Ecn (eV) | 1.369±0.002 | 1.527± 0.003 | 1.58± 0.08 | 1.88± 0.02 | 2.45± 0.04 | 3.14± 0.04 | 4.6± 0.1 | 5.9± 0.1 |
| θn (˚) | -34 ± 9 | -115 ± 9 | -40 ± 25 | -151 ± 18 | -23 ± 20 | -26 ± 10 | --- | --- |

- x = 0.1

| CPPB | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| An | 2 ± 1 | 17 ± 1 | 25 ± 4 | 19 ± 5 | 11 ± 1 | 12 ± 1 | ± 1 | 3 ± 1 |
| n (eV) | 0.10 ± 0.03 | 0.100 ± 0.005 | 0.030 ± 0.004 | 0.20 ± 0.01 | 0.92 ± 0.08 | 1.0 ± 0.1 | 0.9 ± 0.5 | 2 ± 1 |
| Ecn (eV) | 1.43±0.02 | 1.565± 0.002 | 1.740± 0.002 | 1.812± 0.005 | 2.50± 0.04 | 3.1± 0.4 | 4.57± 0.01 | 6.3± 0.7 |
| θn (˚) | -86 ± 40 | -73 ± 5 | -130 ± 10 | -18 ± 5 | -17 ± 5 | -43 ± 12 | --- | --- |

- x = 0.2

| CPPB | 1 | 2 | 3 | 4 | 5 |
| --- | --- | --- | --- | --- | --- |
| An | 11.5 ± 0.4 | 10.0± 0.4 | 11.1±0.3 | 2.4± 0.3 | 4 ± 1 |
| n (eV) | 0.12 ± 0.003 | 0.54 ± 0.002 | 1.13 ± 0.03 | 1.2 ± 0.2 | 1.5 ± 0.3 |
| Ecn (eV) | 1.585±0.002 | 2.56±0.01 | 3.15±0.02 | 4.59±0.04 | 5.89±0.06 |
| θn (˚) | -92±2 | 34±5 | -13±6 | --- | --- |

- x = 0.3

| CPPB | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| An | 2.0 ± 0.4 | 7.9 ± 0.7 | 9 ± 1 | 3.1 ± 0.5 | 8.8 ± 0.5 | 9.4 ± 0.5 | 2.6 ± 0.5 | 3.9 ± 1.2 |
| n (eV) | 0.15 ± 0.03 | 0.1 ± 0.01 | 0.07± 0.01 | 0.20 ± 0.04 | 0.54 ± 0.03 | 1.2 ± 0.08 | 1.5 ± 0.4 | 1.4 ± 0.5 |
| Ecn (eV) | 1.39 ± 0.02 | 1.587 ± 0.005 | 1.795 ± 0.004 | 2.07 ± 0.01 | 2.57 ± 0.02 | 3.22 ± 0.01 | 4.58 ± 0.08 | 5.9 ± 0.1 |
| θn (˚) | -129 ± 24 | -89 ± 11 | -83 ± 10 | --- | 33 ± 10 | --- | --- | --- |

- x = 0.4

| CPPB | 1 | 2 | 3 | 4 | 5 | 6 |
| --- | --- | --- | --- | --- | --- | --- |
| An | 3.7 ± 0.4 | 8.4 ± 0.6 | 8.8 ± 0.5 | 10.7 ± 0.7 | 2.6 ± 0.6 | 5 ± 1 |
| n (eV) | 0.27 ± 0.03 | 0.10 ± 0.01 | 0.53 ± 0.04 | 1.0 ± 0.1 | 3 ± 1 | 0.9 ± 0.3 |
| Ecn (eV) | 1.50 ± 0.07 | 1.66 ± 0.05 | 2.62 ± 0.02 | 3.34 ± 0.04 | 4.5 ± 0.2 | 5.86 ± 0.04 |
| θn (˚) | -96 ± 13 | -65 ± 10 | 36 ± 8 | -20 ± 8 | --- | --- |

Device Performance

EQE simulations are performed using structure parameters and optical properties as the input parameters of all the component materials of FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite-based solar cells. EQE simulations for varying Cs concentration are shown in Fig. S3. The short wavelength EQE and photocurrent for all compositions are looks similar, whereas at longer wavelengths, FA1-xCsxPbI3 perovskite-based solar cells other than x = 2 show significant photocurrent due to sub-band gap absorption. The experimental device performance of FA1-xCsxPbI3 (x = 0.05, 0.1, 0.15, 0.2, 0.25, 0.3) are presented in Table S2.

Table S2. Device performance parameters of FA1-xCsxPbI3 perovskite based solar cells under AM1.5G illumination at reverse and forward voltage scans [1, 2]. *Indicates a film of that composition optically characterized by spectroscopic ellipsometry.

| x | Reverse/ Forward | Voc (V) | Jsc (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| 0* | Reverse | 0.94±0.03 | 22.42±0.93 | 58.44±6.39 | 12.31±1.42 |
|  | Forward | 0.90±0.04 | 22.46±0.80 | 55.56±6.29 | 11.31±1.54 |
| 0.05 | Reverse | 0.94±0.03 | 21.66±0.03 | 63.37±2.06 | 12.94±0.79 |
|  | Forward | 0.93±0.04 | 21.69±0.65 | 58.52±6.93 | 11.79±1.75 |
| 0.1* | Reverse | 0.99±0.01 | 21.80±0.44 | 71.67±0.81 | 15.40±0.33 |
|  | Forward | 0.92±0.01 | 21.87±0.43 | 67.69±0.22 | 13.69±0.19 |
| 0.15 | Reverse | 1.01±0.03 | 21.55±0.18 | 72.13±1.30 | 15.75±0.63 |
|  | Forward | 0.98±0.02 | 21.51±0.18 | 64.39±3.45 | 13.55±0.53 |
| 0.2* | Reverse | 1.03±0.02 | 21.73±0.51 | 72.37±1.18 | 16.18±0.50 |
|  | Forward | 0.97±0.02 | 21.51±0.60 | 64.42±1.71 | 13.45±0.78 |
| 0.25 | Reverse | 1.01±0.03 | 20.83±0.14 | 74.63±2.11 | 15.68±0.84 |
|  | Forward | 0.99±0.03 | 20.74±0.15 | 66.36±3.93 | 13.68±1.06 |
| 0.3* | Reverse | 1.03±0.03 | 20.33±0.34 | 72.48±0.83 | 15.21±0.29 |
|  | Forward | 1.02±0.03 | 20.46±0.53 | 66.20±2.90 | 13.81±0.67 |

Fig. S3. EQE simulations of solar cells with FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite absorbers.

Table S3. Numerically inverted spectra in ε as functions of photon energy for FA1-xCsxPbI3 (x = 0.0, 0.1, 0.2, 0.3, 0.4) perovskite thin films.

- ε for FAPbI3 vs photon energy (eV)

Photon Energy (eV)	ε1	ε2

5.886830	2.026507	3.373881

5.842581	2.161760	3.458311

5.798990	2.264156	3.346755

5.756044	2.304424	3.369601

5.713730	2.363295	3.261392

5.672031	2.408411	3.212655

5.630938	2.469782	3.093170

5.590435	2.555760	3.029248

5.550508	2.538466	2.989153

5.511149	2.544095	2.890448

5.472343	2.482910	2.817760

5.434079	2.494895	2.832765

5.396346	2.513909	2.807997

5.359134	2.485968	2.728368

5.322429	2.443165	2.689920

5.286224	2.447134	2.675419

5.250508	2.377918	2.613849

5.215272	2.335562	2.609549

5.180504	2.287068	2.570335

5.146196	2.245966	2.576081

5.112340	2.201081	2.561360

5.078925	2.164264	2.587555

5.045945	2.147051	2.590020

5.013389	2.090143	2.577167

4.981251	2.087047	2.660778

4.949521	2.056093	2.661617

4.918193	2.021872	2.696930

4.887259	2.001998	2.704611

4.856710	1.972987	2.738702

4.826542	1.954434	2.748396

4.796745	1.966328	2.809556

4.767314	1.956474	2.838899

4.738242	1.950101	2.876668

4.709521	1.988746	2.901558

4.681147	1.989137	2.918075

4.653112	2.021205	2.943039

4.625410	2.013113	2.987797

4.598037	2.031880	2.939823

4.570985	2.031467	2.972214

4.544249	2.043392	2.990176

4.517825	2.036455	2.979219

4.491704	2.045669	2.978347

4.465886	2.034162	2.969577

4.440361	2.039148	2.962280

4.415126	2.053506	2.989478

4.390176	2.015206	2.951329

4.365508	2.006048	2.981326

4.341113	2.004101	2.976391

4.316990	1.984949	2.977107

4.293134	1.952174	2.977178

4.269539	1.937039	2.979446

4.246203	1.910206	2.995738

4.223120	1.889204	3.009526

4.200286	1.882626	3.020718

4.177698	1.829036	3.044630

4.155352	1.817127	3.068207

4.133243	1.796320	3.087177

4.111368	1.747640	3.114187

4.089723	1.725547	3.144196

4.068305	1.692683	3.159528

4.047110	1.648410	3.185669

4.026134	1.613484	3.228929

4.005375	1.581477	3.255501

3.984829	1.545562	3.291356

3.964492	1.518009	3.343941

3.944361	1.479401	3.388871

3.924434	1.440971	3.430352

3.904708	1.405406	3.501861

3.885178	1.365238	3.561970

3.865843	1.344881	3.618661

3.846699	1.315428	3.689242

3.827744	1.270743	3.773366

3.808975	1.265882	3.841319

3.790389	1.237458	3.935471

3.771983	1.215757	4.005039

3.753756	1.212371	4.094881

3.735703	1.201144	4.187966

3.717823	1.185155	4.281471

3.700114	1.173088	4.378654

3.682572	1.177785	4.485553

3.665196	1.198411	4.572524

3.647983	1.206970	4.695432

3.630931	1.220370	4.771160

3.614038	1.243747	4.869321

3.597301	1.265904	5.002470

3.580719	1.317002	5.110075

3.564288	1.369816	5.190828

3.548008	1.398746	5.300989

3.531876	1.443188	5.405902

3.515889	1.500341	5.511501

3.500047	1.573132	5.607767

3.484347	1.649499	5.692133

3.468787	1.722261	5.807839

3.453366	1.793574	5.902432

3.438081	1.873326	5.987660

3.422931	1.955301	6.067620

3.407914	2.069387	6.152772

3.393028	2.172671	6.240787

3.378271	2.282853	6.315939

3.363643	2.388293	6.376154

3.349140	2.507477	6.461026

3.334762	2.608456	6.537893

3.320507	2.721926	6.574440

3.306374	2.842443	6.633773

3.292360	2.972656	6.679274

3.278465	3.087713	6.703749

3.264686	3.224117	6.758166

3.251023	3.344074	6.796797

3.237473	3.499435	6.827803

3.224037	3.626139	6.808940

3.210711	3.787791	6.816937

3.197495	3.917883	6.824684

3.184388	4.055897	6.818041

3.171387	4.185461	6.779748

3.158493	4.289618	6.770314

3.145703	4.446671	6.750329

3.133016	4.559238	6.719597

3.120431	4.666917	6.668719

3.107947	4.781703	6.622555

3.095562	4.880074	6.575634

3.083276	4.992204	6.537685

3.071087	5.086788	6.460391

3.058994	5.190046	6.421086

3.046996	5.262655	6.331442

3.035092	5.339199	6.259690

3.023281	5.441578	6.168261

3.011561	5.518159	6.090832

2.999932	5.560035	6.003334

2.988392	5.630270	5.925219

2.976941	5.663098	5.830594

2.965577	5.717845	5.772961

2.954300	5.747788	5.677109

2.943108	5.781863	5.597877

2.932001	5.787639	5.522961

2.920978	5.828550	5.426921

2.910037	5.814722	5.382565

2.899178	5.831543	5.315187

2.888400	5.830218	5.261621

2.877702	5.834642	5.185956

2.867082	5.829688	5.159622

2.856541	5.832775	5.106108

2.846077	5.833622	5.042557

2.835690	5.824605	5.028135

2.825378	5.805749	4.985852

2.815142	5.800743	4.964245

2.804979	5.803455	4.929393

2.794889	5.786712	4.900911

2.784872	5.778758	4.897126

2.774927	5.793736	4.881573

2.765052	5.765494	4.850384

2.755248	5.763669	4.847374

2.745512	5.762182	4.844189

2.735846	5.763593	4.852767

2.726248	5.762827	4.859061

2.716716	5.771502	4.867609

2.707252	5.783268	4.848023

2.697853	5.778815	4.877912

2.688519	5.782382	4.879020

2.679250	5.790663	4.889262

2.670044	5.817006	4.884961

2.660902	5.835413	4.916171

2.651822	5.864105	4.930339

2.642804	5.884214	4.938374

2.633847	5.921041	4.949800

2.624951	5.954230	4.966678

2.616115	5.976243	4.979352

2.607338	6.014214	4.987458

2.598620	6.042794	4.989015

2.589961	6.109176	4.991531

2.581358	6.136021	5.014322

2.572814	6.182308	5.017162

2.564325	6.227161	5.021006

2.555892	6.275302	5.013025

2.547515	6.332860	5.015899

2.539193	6.397165	5.017907

2.530925	6.450319	4.991690

2.522711	6.496292	5.002141

2.514550	6.553293	4.977459

2.506442	6.603760	4.992199

2.498386	6.665654	4.946814

2.490382	6.725443	4.931923

2.482429	6.788447	4.928402

2.474527	6.829120	4.886109

2.466675	6.880139	4.853436

2.458873	6.921681	4.796122

2.451120	6.987993	4.778780

2.443417	7.052143	4.738961

2.435761	7.098017	4.696672

2.428154	7.123297	4.649787

2.420594	7.184954	4.608747

2.413081	7.231646	4.559000

2.405614	7.272338	4.514297

2.398194	7.310257	4.442380

2.390820	7.312984	4.390738

2.383491	7.364556	4.348435

2.376207	7.400144	4.301656

2.368967	7.433879	4.247736

2.361772	7.463344	4.177411

2.354620	7.484540	4.148787

2.347511	7.508665	4.096899

2.340446	7.523756	4.027540

2.333423	7.543314	3.962698

2.326442	7.560134	3.900812

2.319503	7.569514	3.859594

2.312605	7.569905	3.786547

2.305749	7.578449	3.725972

2.298933	7.555965	3.680360

2.292157	7.573459	3.631492

2.285422	7.552402	3.560151

2.278726	7.565185	3.504266

2.272069	7.541488	3.464954

2.265451	7.541181	3.418511

2.258872	7.503896	3.364548

2.252331	7.493188	3.332458

2.245827	7.492517	3.282607

2.239362	7.476697	3.258769

2.232934	7.465094	3.229510

2.226542	7.435072	3.194932

2.220187	7.429313	3.168572

2.213869	7.403514	3.137354

2.207587	7.383492	3.111981

2.201340	7.372086	3.101527

2.195129	7.363070	3.070817

2.188952	7.336279	3.056495

2.182811	7.321166	3.042130

2.176704	7.312150	3.021633

2.170631	7.291008	2.988457

2.164593	7.299025	2.999182

2.158587	7.303378	2.984329

2.152616	7.276141	2.963012

2.146677	7.268326	2.952506

2.140771	7.288920	2.949694

2.134898	7.270259	2.934287

2.129057	7.270986	2.931530

2.123248	7.280402	2.912911

2.117471	7.266901	2.895745

2.111725	7.263241	2.880825

2.106011	7.276207	2.878564

2.100327	7.272063	2.847733

2.094674	7.272709	2.833981

2.089052	7.257264	2.817461

2.083460	7.258865	2.807387

2.077898	7.262411	2.792747

2.072366	7.253923	2.776494

2.066863	7.247917	2.767395

2.061389	7.269529	2.760583

2.055945	7.267828	2.746077

2.050529	7.262381	2.733268

2.045143	7.265954	2.708337

2.039784	7.279630	2.707828

2.034454	7.276451	2.689994

2.029151	7.261032	2.666866

2.023876	7.276829	2.655992

2.018629	7.286091	2.643803

2.013409	7.291362	2.621926

2.008216	7.280345	2.608139

2.003050	7.303131	2.597999

1.997911	7.304153	2.575811

1.992798	7.307132	2.556982

1.987711	7.327978	2.535819

1.982651	7.326489	2.521710

1.977616	7.340641	2.494390

1.972607	7.332407	2.471970

1.967623	7.342909	2.439782

1.962664	7.352484	2.410825

1.957731	7.366020	2.380083

1.952823	7.341306	2.335535

1.947939	7.353130	2.303511

1.943080	7.351268	2.275111

1.938245	7.322527	2.231087

1.933434	7.322466	2.203055

1.928647	7.299399	2.169297

1.923884	7.292297	2.136531

1.919145	7.281166	2.117330

1.914429	7.260493	2.075257

1.909737	7.237745	2.045504

1.905067	7.217169	2.019726

1.900420	7.176993	1.981590

1.895796	7.160008	1.956147

1.891195	7.128733	1.930807

1.886616	7.093555	1.896399

1.882060	7.075347	1.890419

1.877525	7.006553	1.858634

1.873013	6.960914	1.832330

1.868522	6.911957	1.844970

1.864053	6.848279	1.835905

1.859605	6.830127	1.844950

1.855179	6.762061	1.862052

1.850774	6.691626	1.869689

1.846390	6.645903	1.906502

1.842026	6.642020	1.920978

1.837684	6.616543	1.952582

1.833362	6.596169	1.983317

1.829061	6.572528	2.009021

1.824779	6.551441	2.031353

1.820518	6.544139	2.057638

1.816277	6.546997	2.083460

1.812056	6.523601	2.111524

1.807855	6.498280	2.131973

1.803673	6.493057	2.160468

1.799510	6.498465	2.182728

1.795367	6.485794	2.204066

1.791243	6.484025	2.235459

1.787138	6.476782	2.253189

1.783052	6.469449	2.275063

1.778985	6.482632	2.309895

1.774937	6.482524	2.328515

1.770907	6.486824	2.355295

1.766895	6.508878	2.381387

1.762902	6.484766	2.404323

1.758927	6.493303	2.423854

1.754970	6.516112	2.449145

1.751030	6.512002	2.473683

1.747109	6.513497	2.485912

1.743205	6.541373	2.513801

1.739319	6.568557	2.539573

1.735450	6.580125	2.563753

1.731599	6.587502	2.578948

1.727765	6.595162	2.597419

1.723948	6.638259	2.625636

1.720148	6.652020	2.634655

1.716365	6.674492	2.655504

1.712598	6.680668	2.673592

1.708848	6.703780	2.683769

1.705115	6.739005	2.702238

1.701398	6.758003	2.718360

1.697697	6.772530	2.729452

1.694013	6.809010	2.731843

1.690345	6.828261	2.745962

1.686693	6.850381	2.753659

1.683056	6.879801	2.767889

1.679436	6.916163	2.776861

1.675831	6.939160	2.782162

1.672242	6.961431	2.785561

1.668668	6.981971	2.789361

1.665109	7.038107	2.809169

1.661566	7.037776	2.793299

1.658038	7.086831	2.798183

1.654526	7.122544	2.807395

1.651028	7.136825	2.799515

1.647545	7.169899	2.793119

1.644077	7.217292	2.802001

1.640624	7.226059	2.798690

1.637185	7.263275	2.791101

1.633761	7.288737	2.785359

1.630351	7.324003	2.785412

1.626956	7.355283	2.768597

1.623574	7.394223	2.759413

1.620207	7.409570	2.759172

1.616855	7.448105	2.751625

1.613516	7.462342	2.743083

1.610191	7.483077	2.726198

1.606880	7.515806	2.717194

1.603582	7.582134	2.703097

1.600299	7.597785	2.696674

1.597028	7.613309	2.677156

1.593772	7.648637	2.661646

1.590528	7.664037	2.645782

1.587298	7.740826	2.650279

1.584082	7.746187	2.636067

1.580878	7.813974	2.613344

1.577688	7.813999	2.597164

1.574510	7.848932	2.573724

1.571346	7.898213	2.542893

1.568194	7.952856	2.527745

1.565055	8.004516	2.509036

1.561929	8.011484	2.471495

1.558815	8.069410	2.424001

1.555714	8.157134	2.388262

1.552625	8.188532	2.338849

1.549549	8.225248	2.293854

1.546485	8.248804	2.222928

1.543433	8.281648	2.155655

1.540394	8.290983	2.076765

1.537367	8.326528	1.981470

1.534351	8.344033	1.883135

1.531348	8.325213	1.801593

1.528356	8.307902	1.721288

1.525376	8.269814	1.652794

1.522408	8.247632	1.582672

1.519452	8.201000	1.518743

1.516507	8.158903	1.454892

1.513574	8.099281	1.398089

1.510652	8.051931	1.348929

1.507742	8.016654	1.321494

1.504843	8.012322	1.312609

1.501955	8.002433	1.302864

1.499079	7.974257	1.281331

1.496213	7.931098	1.256198

1.493359	7.907219	1.243787

1.490516	7.877526	1.233700

1.487683	7.813106	1.208267

1.484862	7.776315	1.192655

1.482051	7.762943	1.184331

1.479252	7.742605	1.180965

1.476462	7.687804	1.174791

1.473684	7.645645	1.160157

1.470916	7.636673	1.161965

1.468159	7.618161	1.156353

1.465412	7.582959	1.161814

1.462675	7.562049	1.160335

1.459949	7.534202	1.163031

1.457233	7.501330	1.161254

1.454528	7.456617	1.150481

1.451832	7.420915	1.159026

1.449147	7.401452	1.158333

1.446472	7.362464	1.156885

1.443806	7.339140	1.160855

1.441151	7.311495	1.159489

1.438506	7.295883	1.170100

1.435870	7.242300	1.144652

1.433244	7.217930	1.160342

1.430628	7.206248	1.162420

1.428022	7.179904	1.160906

1.425425	7.145010	1.165475

1.422838	7.125269	1.173221

1.420260	7.094480	1.169861

1.417692	7.064162	1.164594

1.415133	7.032493	1.169863

1.412584	7.006479	1.177839

1.410044	6.964470	1.177653

1.407513	6.932504	1.170275

1.404991	6.928898	1.171631

1.402479	6.933085	1.163761

1.399975	6.936573	1.165822

1.397481	6.917886	1.164321

1.394996	6.880270	1.173957

1.392519	6.835747	1.192975

1.390052	6.778224	1.201616

1.387594	6.709653	1.222624

1.385144	6.661998	1.224809

1.382703	6.644481	1.215957

1.380271	6.623008	1.226269

1.377847	6.574464	1.232797

1.375432	6.487286	1.240569

1.373026	6.345539	1.219531

1.370628	6.244708	1.166954

1.368239	6.245298	1.123399

1.365858	6.242332	1.087943

1.363486	6.208534	1.051487

1.361122	6.160344	0.965372

1.358766	6.104103	0.869847

1.356419	6.101093	0.793295

1.354080	6.111138	0.752801

1.351749	6.117592	0.728809

1.349426	6.142996	0.718173

1.347111	6.149291	0.699482

1.344805	6.146071	0.672136

1.342506	6.140911	0.649708

1.340216	6.149762	0.628900

1.337933	6.148566	0.600073

1.335658	6.139135	0.577134

1.333391	6.127055	0.539711

1.331132	6.138959	0.517552

1.328881	6.135067	0.489862

1.326638	6.133198	0.473270

1.324402	6.136933	0.449555

1.322173	6.136118	0.424990

1.319953	6.133681	0.406504

1.317740	6.148550	0.393204

1.315535	6.149903	0.380403

1.313337	6.145952	0.360403

1.311146	6.156253	0.353921

1.308963	6.152027	0.333284

1.306788	6.150384	0.313569

1.304619	6.159403	0.305656

1.302459	6.161838	0.295711

1.300305	6.174200	0.291018

1.298159	6.178614	0.282239

1.296019	6.181518	0.274164

1.293887	6.183482	0.265282

1.291763	6.176899	0.250329

1.289645	6.176763	0.242693

1.287534	6.178843	0.236986

1.285431	6.173919	0.223228

1.283334	6.162693	0.197356

1.281244	6.178429	0.197519

1.279162	6.177711	0.184260

1.277086	6.182096	0.177036

1.275017	6.183774	0.170410

1.272955	6.187673	0.162787

1.270900	6.184315	0.149933

1.268851	6.184980	0.141007

1.266809	6.194228	0.139908

1.264774	6.206689	0.136279

1.262746	6.213664	0.127650

1.260724	6.227254	0.128297

1.258709	6.236425	0.123691

1.256700	6.234557	0.117966

1.254698	6.227822	0.113874

1.252702	6.220525	0.104030

1.250713	6.222063	0.093721

1.248730	6.227690	0.090537

1.246754	6.239082	0.090037

1.244784	6.251092	0.086130

1.242821	6.261078	0.087891

1.240863	6.271021	0.086816

1.224385	6.175201	0.049285

1.220322	6.176178	0.031771

1.216285	6.173895	0.022440

1.212273	6.175693	0.009960

1.208287	6.177099	0.020783

1.204326	6.177160	0.004134

1.200390	6.178618	0.014311

1.196478	6.176414	0.004462

1.192591	6.175200	0.014743

1.188727	6.177035	0.000000

1.184888	6.177635	0.002819

1.181073	6.185752	0.000000

1.177281	6.183857	0.000130

1.173512	6.185557	0.000000

1.169767	6.178704	0.000000

1.166045	6.177291	0.000000

1.162345	6.172775	0.000000

1.158667	6.179008	0.000000

1.155012	6.169704	0.000000

1.151380	6.175384	0.000000

1.147769	6.179850	0.000000

1.144179	6.174216	0.000000

1.140612	6.176875	0.000000

1.137066	6.173095	0.000000

1.133540	6.166133	0.000000

1.130036	6.161849	0.000000

1.126553	6.156384	0.000000

1.123090	6.157257	0.000000

1.119648	6.160435	0.000000

1.116226	6.160351	0.000000

1.112824	6.155347	0.000000

1.109442	6.143879	0.000000

1.106080	6.144544	0.000000

1.102737	6.148641	0.000000

1.099414	6.142081	0.000000

1.096110	6.136660	0.000000

1.092825	6.130778	0.000000

1.089559	6.133969	0.000000

1.086312	6.124663	0.000000

1.083084	6.127084	0.000000

1.079874	6.121575	0.000000

1.076682	6.117592	0.000000

1.073509	6.111821	0.000000

1.070353	6.106616	0.000000

1.067216	6.105271	0.000000

1.064096	6.089182	0.000000

1.060994	6.090825	0.000000

1.057909	6.095647	0.000000

1.054841	6.090669	0.000000

1.051791	6.083610	0.000000

1.048758	6.078282	0.000000

1.045741	6.084847	0.000000

1.042742	6.062524	0.000000

1.039759	6.069623	0.000000

1.036792	6.065921	0.000000

1.033842	6.053887	0.000000

1.030908	6.049835	0.000000

1.027990	6.045391	0.000000

1.025088	6.023739	0.000000

1.022202	6.035344	0.000000

1.019331	6.009983	0.000000

1.016477	6.027351	0.000000

1.013637	6.012287	0.000000

1.010813	6.007568	0.000000

1.008005	6.001776	0.000000

1.005211	5.985655	0.000000

1.002432	5.994017	0.000000

0.999669	5.982446	0.000000

0.996920	5.991334	0.000000

0.994185	5.978168	0.000000

0.991465	5.960916	0.000000

0.988760	5.944091	0.000000

0.986069	5.944763	0.000000

0.983392	5.948592	0.000000

0.980729	5.948767	0.000000

0.978081	5.930645	0.000000

0.975446	5.922457	0.000000

0.972825	5.898432	0.000000

0.970217	5.902441	0.000000

0.967623	5.887526	0.000000

0.965043	5.901319	0.000000

0.962476	5.870509	0.000000

0.959922	5.873239	0.000000

0.957382	5.863016	0.000000

0.954855	5.858070	0.000000

0.952340	5.854822	0.000000

0.949839	5.848248	0.000000

0.947350	5.839207	0.000000

0.944874	5.827389	0.000000

0.942410	5.822940	0.000000

0.939959	5.814989	0.000000

0.937521	5.803179	0.000000

0.935095	5.796233	0.000000

0.932681	5.791955	0.000000

0.930279	5.782634	0.000000

0.927889	5.759095	0.000000

0.925512	5.748550	0.000000

0.923146	5.772812	0.000000

0.920792	5.743893	0.000000

0.918449	5.726087	0.000000

0.916119	5.742655	0.000000

0.913800	5.719948	0.000000

0.911492	5.718547	0.000000

0.909196	5.718497	0.000000

0.906911	5.721543	0.000000

0.904637	5.706049	0.000000

0.902375	5.699324	0.000000

0.900123	5.711452	0.000000

0.897883	5.669612	0.000000

0.895653	5.688004	0.000000

0.893435	5.647842	0.000000

0.891227	5.656990	0.000000

0.889030	5.641398	0.000000

0.886843	5.632232	0.000000

0.884667	5.650050	0.000000

0.882502	5.642356	0.000000

0.880347	5.613808	0.000000

0.878202	5.621256	0.000000

0.876067	5.617734	0.000000

0.873943	5.597004	0.000000

0.871829	5.606742	0.000000

0.869725	5.588210	0.000000

0.867630	5.598918	0.000000

0.865546	5.586082	0.000000

0.863472	5.574775	0.000000

0.861407	5.547540	0.000000

0.859352	5.565798	0.000000

0.857307	5.547717	0.000000

0.855272	5.520281	0.000000

0.853245	5.550951	0.000000

0.851229	5.556255	0.000000

0.849222	5.533556	0.000000

0.847224	5.536878	0.000000

0.845235	5.526581	0.000000

0.843256	5.528271	0.000000

0.841285	5.536305	0.000000

0.839324	5.537861	0.000000

0.837372	5.546738	0.000000

0.835429	5.505408	0.000000

0.833495	5.514678	0.000000

0.831570	5.512758	0.000000

0.829653	5.532440	0.000000

0.827745	5.485871	0.000000

0.825846	5.449689	0.000000

0.823956	5.518289	0.000000

0.822074	5.482044	0.000000

0.820200	5.481231	0.000000

0.818335	5.516076	0.000000

0.816479	5.546496	0.000000

0.814631	5.475219	0.000000

0.812791	5.517077	0.000000

0.810959	5.484996	0.000000

0.809136	5.515436	0.000000

0.807321	5.475062	0.000000

0.805514	5.481056	0.000000

0.803715	5.466012	0.000000

0.801923	5.521731	0.000000

0.800140	5.489605	0.000000

0.798365	5.509077	0.000000

0.796598	5.437933	0.000000

0.794838	5.474157	0.000000

0.793086	5.479352	0.000000

0.791342	5.506790	0.000000

0.789605	5.427752	0.000000

0.787876	5.502966	0.000000

0.786155	5.398276	0.000000

0.784441	5.479343	0.000000

0.782735	5.479519	0.000000

0.781036	5.519258	0.000000

0.779344	5.421347	0.000000

0.777660	5.492322	0.000000

0.775983	5.477025	0.000000

0.774313	5.481864	0.000000

0.772651	5.463862	0.000000

0.770995	5.450783	0.000000

0.769347	5.463323	0.000000

0.767706	5.575143	0.000000

0.766072	5.506457	0.000000

0.764444	5.492317	0.000000

0.762824	5.489245	0.000000

0.761211	5.467572	0.000000

0.759604	5.472315	0.000000

0.758004	5.529541	0.000000

0.756411	5.466303	0.000000

0.754825	5.499017	0.000000

0.753246	5.436095	0.000000

0.751673	5.425173	0.000000

0.750107	5.557410	0.000000

0.748547	5.470019	0.000000

0.746994	5.469498	0.000000

0.745447	5.521831	0.000000

0.743907	5.515370	0.000000

0.742373	5.484842	0.000000

0.740846	5.501848	0.000000

0.739325	5.368865	0.000000

0.737810	5.493109	0.000000

0.736301	5.462239	0.000000

0.734799	5.490098	0.000000

- ε for FA0.9Cs0.1PbI3 vs photon energy (eV)

Photon Energy (eV) 	ε1	ε2

5.886830	1.860925	2.923028

5.842581	2.042951	2.815362

5.798990	1.983857	2.738496

5.756044	2.024741	2.723640

5.713730	2.099541	2.633741

5.672031	2.167094	2.726415

5.630938	2.162252	2.621247

5.590435	2.180194	2.586627

5.550508	2.177055	2.523266

5.511149	2.199319	2.463306

5.472343	2.210929	2.415901

5.434079	2.207015	2.360761

5.396346	2.162897	2.312130

5.359134	2.134875	2.258108

5.322429	2.126405	2.262169

5.286224	2.084432	2.220243

5.250508	2.060831	2.181831

5.215272	2.058733	2.176109

5.180504	1.968714	2.171500

5.146196	1.954271	2.173087

5.112340	1.949822	2.171222

5.078925	1.892742	2.171534

5.045945	1.869487	2.188229

5.013389	1.825942	2.184769

4.981251	1.801824	2.221948

4.949521	1.780201	2.235271

4.918193	1.754593	2.250666

4.887259	1.721325	2.279226

4.856710	1.727175	2.331413

4.826542	1.703984	2.353209

4.796745	1.700738	2.372444

4.767314	1.711095	2.422393

4.738242	1.705234	2.447143

4.709521	1.713562	2.449916

4.681147	1.719593	2.466935

4.653112	1.727208	2.495771

4.625410	1.739380	2.519917

4.598037	1.740199	2.522167

4.570985	1.754852	2.549949

4.544249	1.766435	2.546506

4.517825	1.771570	2.551247

4.491704	1.776198	2.563406

4.465886	1.776988	2.555344

4.440361	1.764849	2.553850

4.415126	1.773875	2.560348

4.390176	1.755253	2.563146

4.365508	1.749379	2.550018

4.341113	1.746929	2.555951

4.316990	1.738492	2.556518

4.293134	1.731806	2.562047

4.269539	1.711609	2.567473

4.246203	1.701213	2.576916

4.223120	1.668970	2.580983

4.200286	1.653592	2.587990

4.177698	1.623264	2.609636

4.155352	1.594422	2.621350

4.133243	1.573429	2.637176

4.111368	1.551945	2.648682

4.089723	1.526129	2.660852

4.068305	1.485596	2.694615

4.047110	1.472202	2.714725

4.026134	1.436932	2.752356

4.005375	1.420843	2.770050

3.984829	1.373988	2.797323

3.964492	1.347447	2.834026

3.944361	1.319925	2.865509

3.924434	1.283530	2.897906

3.904708	1.256357	2.946491

3.885178	1.221761	2.994924

3.865843	1.201399	3.053844

3.846699	1.161126	3.107994

3.827744	1.138572	3.172845

3.808975	1.111270	3.221451

3.790389	1.085860	3.299050

3.771983	1.067277	3.359679

3.753756	1.051788	3.434353

3.735703	1.034556	3.506361

3.717823	1.019398	3.573777

3.700114	1.028028	3.666449

3.682572	1.012632	3.746770

3.665196	1.016271	3.837395

3.647983	1.024354	3.908662

3.630931	1.038285	4.012939

3.614038	1.057831	4.084116

3.597301	1.063642	4.166883

3.580719	1.098518	4.254076

3.564288	1.123005	4.334200

3.548008	1.159210	4.422117

3.531876	1.187815	4.507009

3.515889	1.229993	4.592637

3.500047	1.268534	4.668672

3.484347	1.313880	4.762225

3.468787	1.371652	4.833718

3.453366	1.423784	4.921369

3.438081	1.480127	4.979074

3.422931	1.558352	5.068567

3.407914	1.629821	5.153395

3.393028	1.714976	5.209667

3.378271	1.787131	5.282918

3.363643	1.873015	5.353089

3.349140	1.960923	5.415058

3.334762	2.028884	5.471612

3.320507	2.109674	5.545147

3.306374	2.187118	5.596480

3.292360	2.297470	5.629543

3.278465	2.396043	5.694045

3.264686	2.500368	5.751845

3.251023	2.594356	5.785832

3.237473	2.711018	5.790595

3.224037	2.818972	5.820611

3.210711	2.946085	5.829755

3.197495	3.050563	5.847453

3.184388	3.150070	5.848100

3.171387	3.278388	5.844311

3.158493	3.375814	5.842408

3.145703	3.472356	5.836879

3.133016	3.574080	5.813960

3.120431	3.673379	5.791925

3.107947	3.757433	5.763816

3.095562	3.850396	5.713788

3.083276	3.930862	5.707384

3.071087	4.017609	5.664702

3.058994	4.094789	5.624204

3.046996	4.174985	5.575428

3.035092	4.265105	5.525504

3.023281	4.317261	5.457800

3.011561	4.394712	5.404520

2.999932	4.447251	5.342205

2.988392	4.495024	5.286135

2.976941	4.544241	5.239100

2.965577	4.586879	5.146811

2.954300	4.613042	5.103346

2.943108	4.642374	5.031934

2.932001	4.664640	4.968623

2.920978	4.681160	4.927624

2.910037	4.692584	4.870802

2.899178	4.710361	4.823071

2.888400	4.709739	4.776243

2.877702	4.718477	4.716022

2.867082	4.724135	4.705043

2.856541	4.722542	4.662417

2.846077	4.715047	4.626127

2.835690	4.719347	4.615804

2.825378	4.720877	4.575922

2.815142	4.713416	4.553245

2.804979	4.701817	4.541300

2.794889	4.694933	4.519864

2.784872	4.691698	4.507054

2.774927	4.686372	4.489678

2.765052	4.672453	4.484590

2.755248	4.679456	4.493992

2.745512	4.666298	4.483655

2.735846	4.672590	4.483906

2.726248	4.659256	4.489228

2.716716	4.671236	4.496298

2.707252	4.662230	4.498849

2.697853	4.677855	4.523305

2.688519	4.671748	4.526351

2.679250	4.670216	4.546520

2.670044	4.678071	4.563462

2.660902	4.693480	4.584914

2.651822	4.708498	4.608800

2.642804	4.729356	4.622361

2.633847	4.742350	4.648288

2.624951	4.768881	4.678263

2.616115	4.787487	4.701281

2.607338	4.813573	4.716420

2.598620	4.838295	4.742893

2.589961	4.891646	4.775592

2.581358	4.933475	4.792498

2.572814	4.960026	4.831370

2.564325	4.992225	4.832798

2.555892	5.052056	4.856922

2.547515	5.086529	4.866472

2.539193	5.154359	4.895860

2.530925	5.203664	4.916656

2.522711	5.243275	4.901944

2.514550	5.305561	4.925137

2.506442	5.348027	4.917173

2.498386	5.406239	4.919945

2.490382	5.467500	4.921571

2.482429	5.519319	4.912063

2.474527	5.584065	4.893938

2.466675	5.631383	4.887065

2.458873	5.705156	4.886171

2.451120	5.747854	4.866555

2.443417	5.799461	4.840111

2.435761	5.855118	4.829791

2.428154	5.913915	4.796422

2.420594	5.960843	4.760255

2.413081	6.022494	4.747042

2.405614	6.058355	4.703505

2.398194	6.117329	4.688700

2.390820	6.154383	4.651883

2.383491	6.192696	4.616863

2.376207	6.234482	4.581528

2.368967	6.276721	4.548437

2.361772	6.297356	4.516861

2.354620	6.341520	4.484088

2.347511	6.370344	4.453174

2.340446	6.408904	4.420682

2.333423	6.432409	4.386736

2.326442	6.455695	4.336245

2.319503	6.490414	4.293079

2.312605	6.529723	4.274915

2.305749	6.545531	4.229984

2.298933	6.564143	4.197341

2.292157	6.578453	4.160844

2.285422	6.612973	4.125890

2.278726	6.624156	4.082109

2.272069	6.642955	4.046300

2.265451	6.671628	4.022278

2.258872	6.694671	3.992919

2.252331	6.698896	3.948349

2.245827	6.740249	3.931050

2.239362	6.749152	3.898640

2.232934	6.765622	3.866046

2.226542	6.761836	3.823840

2.220187	6.799192	3.804339

2.213869	6.807108	3.775333

2.207587	6.809591	3.729551

2.201340	6.852581	3.708272

2.195129	6.851702	3.671606

2.188952	6.866813	3.642328

2.182811	6.882904	3.609003

2.176704	6.890633	3.581161

2.170631	6.895963	3.535364

2.164593	6.918423	3.510353

2.158587	6.933095	3.486656

2.152616	6.942579	3.444952

2.146677	6.965693	3.412861

2.140771	6.961816	3.380944

2.134898	6.967906	3.346786

2.129057	6.989728	3.318882

2.123248	6.992068	3.288582

2.117471	6.997297	3.254302

2.111725	7.012024	3.222975

2.106011	7.001927	3.179898

2.100327	7.004608	3.144355

2.094674	7.013931	3.118814

2.089052	7.018241	3.088186

2.083460	6.995053	3.040000

2.077898	7.011930	3.016541

2.072366	6.989662	2.974929

2.066863	6.992772	2.948442

2.061389	6.986113	2.918520

2.055945	6.982106	2.890336

2.050529	6.976476	2.853844

2.045143	6.961901	2.813072

2.039784	6.944338	2.800180

2.034454	6.930977	2.767423

2.029151	6.923659	2.757180

2.023876	6.907274	2.723278

2.018629	6.895346	2.713971

2.013409	6.891350	2.696876

2.008216	6.858286	2.668592

2.003050	6.847250	2.655023

1.997911	6.823905	2.638121

1.992798	6.813781	2.634299

1.987711	6.799022	2.623025

1.982651	6.772767	2.612675

1.977616	6.761374	2.615743

1.972607	6.732845	2.602793

1.967623	6.727300	2.594856

1.962664	6.706247	2.599422

1.957731	6.700683	2.615258

1.952823	6.679386	2.618915

1.947939	6.661844	2.623884

1.943080	6.676899	2.637670

1.938245	6.649017	2.643313

1.933434	6.638925	2.650521

1.928647	6.625488	2.668073

1.923884	6.633745	2.694042

1.919145	6.644043	2.712833

1.914429	6.646502	2.729333

1.909737	6.632246	2.734714

1.905067	6.667027	2.767236

1.900420	6.674558	2.773870

1.895796	6.696175	2.798262

1.891195	6.731243	2.820599

1.886616	6.732815	2.833825

1.882060	6.771833	2.852087

1.877525	6.778941	2.867557

1.873013	6.808336	2.857759

1.868522	6.849973	2.886236

1.864053	6.876372	2.895763

1.859605	6.914329	2.891036

1.855179	6.976581	2.910673

1.850774	6.991181	2.900899

1.846390	7.042747	2.913161

1.842026	7.102146	2.916445

1.837684	7.130738	2.900904

1.833362	7.159325	2.900577

1.829061	7.216362	2.888490

1.824779	7.275298	2.887445

1.820518	7.320468	2.851296

1.816277	7.369112	2.847049

1.812056	7.412152	2.810424

1.807855	7.437812	2.781252

1.803673	7.502579	2.767903

1.799510	7.572622	2.738134

1.795367	7.591892	2.699064

1.791243	7.655922	2.671839

1.787138	7.711892	2.606519

1.783052	7.734938	2.542063

1.778985	7.780639	2.505434

1.774937	7.819786	2.441256

1.770907	7.868551	2.398549

1.766895	7.901424	2.319071

1.762902	7.961058	2.276699

1.758927	7.964544	2.186151

1.754970	8.049091	2.124488

1.751030	8.037279	2.013167

1.747109	8.043386	1.908458

1.743205	8.055112	1.805075

1.739319	7.981220	1.605294

1.735450	7.855644	1.549980

1.731599	7.750441	1.492514

1.727765	7.721577	1.446259

1.723948	7.651165	1.450798

1.720148	7.593897	1.444195

1.716365	7.554527	1.430292

1.712598	7.488984	1.448745

1.708848	7.480020	1.429844

1.705115	7.460585	1.411379

1.701398	7.431840	1.421452

1.697697	7.411337	1.398212

1.694013	7.392157	1.398346

1.690345	7.376486	1.395526

1.686693	7.372592	1.379914

1.683056	7.353154	1.383876

1.679436	7.336580	1.381077

1.675831	7.321014	1.372078

1.672242	7.317739	1.365194

1.668668	7.296625	1.367046

1.665109	7.284935	1.364081

1.661566	7.278747	1.358705

1.658038	7.277531	1.357136

1.654526	7.262338	1.353979

1.651028	7.261382	1.351504

1.647545	7.250872	1.345545

1.644077	7.252320	1.343490

1.640624	7.250840	1.336509

1.637185	7.257645	1.331529

1.633761	7.259370	1.330280

1.630351	7.260719	1.325986

1.626956	7.265532	1.326935

1.623574	7.270170	1.321087

1.620207	7.272919	1.317878

1.616855	7.293890	1.309778

1.613516	7.298830	1.312806

1.610191	7.298651	1.301674

1.606880	7.326085	1.292530

1.603582	7.340007	1.282894

1.600299	7.346142	1.273852

1.597028	7.364904	1.254036

1.593772	7.390110	1.239874

1.590528	7.412271	1.216041

1.587298	7.432187	1.192651

1.584082	7.477059	1.162400

1.580878	7.486333	1.131891

1.577688	7.503849	1.089448

1.574510	7.538826	1.034029

1.571346	7.549701	0.973928

1.568194	7.569801	0.931499

1.565055	7.567447	0.879432

1.561929	7.565305	0.822456

1.558815	7.544218	0.751425

1.555714	7.529467	0.687104

1.552625	7.512455	0.636154

1.549549	7.484463	0.593842

1.546485	7.449419	0.542915

1.543433	7.412290	0.497550

1.540394	7.374156	0.458259

1.537367	7.330850	0.420765

1.534351	7.289903	0.390979

1.531348	7.248349	0.361857

1.528356	7.209131	0.339802

1.525376	7.169196	0.321369

1.522408	7.126922	0.302939

1.519452	7.090376	0.289851

1.516507	7.043086	0.271886

1.513574	6.997172	0.254433

1.510652	6.956467	0.240579

1.507742	6.940045	0.228064

1.504843	6.939060	0.219855

1.501955	6.937938	0.214316

1.499079	6.919645	0.209382

1.496213	6.893773	0.204790

1.493359	6.881295	0.198200

1.490516	6.860562	0.196455

1.487683	6.818281	0.193539

1.484862	6.790770	0.188355

1.482051	6.785891	0.182076

1.479252	6.778732	0.180106

1.476462	6.748832	0.182257

1.473684	6.723464	0.177573

1.470916	6.713432	0.174056

1.468159	6.704370	0.173695

1.465412	6.690665	0.172009

1.462675	6.665282	0.175052

1.459949	6.641817	0.173446

1.457233	6.616674	0.170454

1.454528	6.595508	0.168013

1.451832	6.575907	0.168004

1.449147	6.554949	0.160788

1.446472	6.541382	0.157239

1.443806	6.521454	0.152177

1.441151	6.503099	0.146060

1.438506	6.490389	0.140787

1.435870	6.471605	0.134210

1.433244	6.460912	0.130267

1.430628	6.448833	0.118543

1.428022	6.442291	0.114687

1.425425	6.437682	0.107178

1.422838	6.420973	0.102750

1.420260	6.412603	0.095527

1.417692	6.403893	0.091264

1.415133	6.394168	0.086611

1.412584	6.383234	0.078827

1.410044	6.368626	0.072862

1.407513	6.370166	0.066569

1.404991	6.377690	0.063386

1.402479	6.389715	0.059043

1.399975	6.399620	0.057345

1.397481	6.401524	0.055514

1.394996	6.389514	0.054886

1.392519	6.374492	0.052528

1.390052	6.359312	0.049574

1.387594	6.339947	0.045206

1.385144	6.331255	0.040080

1.382703	6.339873	0.038275

1.380271	6.342975	0.035733

1.377847	6.340436	0.035468

1.375432	6.323224	0.034564

1.373026	6.307254	0.030853

1.370628	6.298989	0.026954

1.368239	6.309359	0.025653

1.365858	6.313871	0.021153

1.363486	6.315639	0.021631

1.361122	6.304738	0.021230

1.358766	6.280347	0.017961

1.356419	6.263466	0.015805

1.354080	6.263981	0.011378

1.351749	6.267798	0.008630

1.349426	6.277418	0.006576

1.347111	6.284159	0.004616

1.344805	6.288685	0.007537

1.342506	6.288418	0.006456

1.340216	6.285578	0.008784

1.337933	6.276412	0.003752

1.335658	6.271464	0.004137

1.333391	6.272531	0.014168

1.331132	6.255572	0.008081

1.328881	6.248576	0.003081

1.326638	6.242665	0.006009

1.324402	6.224678	-0.008225

1.322173	6.222699	-0.002090

1.319953	6.226174	-0.003052

1.317740	6.225125	-0.001637

1.315535	6.219281	-0.007193

1.313337	6.218040	-0.004890

1.311146	6.210738	-0.007470

1.308963	6.206542	-0.011528

1.306788	6.197004	-0.009301

1.304619	6.198931	-0.005836

1.302459	6.195884	-0.013331

1.300305	6.195655	-0.013922

1.298159	6.193946	-0.018340

1.296019	6.198270	-0.005752

1.293887	6.191587	-0.015078

1.291763	6.188864	0.002109

1.289645	6.176584	-0.018273

1.287534	6.169224	-0.006081

1.285431	6.159875	-0.007728

1.283334	6.149807	-0.012725

1.281244	6.146384	-0.016464

1.279162	6.145969	-0.012359

1.277086	6.139029	-0.008959

1.275017	6.136962	-0.022252

1.272955	6.136720	-0.014322

1.270900	6.129385	-0.019032

1.268851	6.122812	-0.017155

1.266809	6.125769	-0.019046

1.264774	6.137978	-0.020676

1.262746	6.144115	-0.018814

1.260724	6.149646	-0.019551

1.258709	6.158261	-0.017606

1.256700	6.153930	-0.014700

1.254698	6.138634	-0.022719

1.252702	6.127177	-0.019576

1.250713	6.122540	-0.016901

1.248730	6.124587	-0.019797

1.246754	6.129678	-0.022725

1.244784	6.138444	-0.017586

1.242821	6.148244	-0.027074

1.240863	6.154948	-0.021699

1.224385	6.002085	-0.013242

1.220322	5.993912	-0.007795

1.216285	5.990195	-0.022094

1.212273	5.978454	-0.011550

1.208287	5.973068	-0.014572

1.204326	5.971663	-0.005807

1.200390	5.964615	-0.010077

1.196478	5.957935	-0.015613

1.192591	5.948575	-0.008510

1.188727	5.941906	-0.009617

1.184888	5.947868	-0.013699

1.181073	5.941966	-0.013607

1.177281	5.934075	-0.010928

1.173512	5.931440	-0.003246

1.169767	5.920369	-0.007356

1.166045	5.918656	-0.010014

1.162345	5.908677	-0.006303

1.158667	5.910933	-0.005847

1.155012	5.897012	-0.006188

1.151380	5.900427	-0.005255

1.147769	5.907115	-0.009303

1.144179	5.892350	-0.006314

1.140612	5.886931	-0.003797

1.137066	5.884190	-0.009851

1.133540	5.880960	-0.002337

1.130036	5.868437	-0.004925

1.126553	5.855403	-0.000842

1.123090	5.864254	-0.004319

1.119648	5.864478	-0.003710

1.116226	5.860235	-0.001890

1.112824	5.849327	-0.000844

1.109442	5.859982	-0.004760

1.106080	5.849097	-0.002520

1.102737	5.833059	-0.002414

1.099414	5.836498	0.006756

1.096110	5.841326	0.006767

1.092825	5.829809	-0.004108

1.089559	5.827322	0.001194

1.086312	5.825387	0.001055

1.083084	5.824646	0.003437

1.079874	5.820119	0.000384

1.076682	5.813706	0.000350

1.073509	5.812557	0.004335

1.070353	5.802395	0.006864

1.067216	5.801149	0.004623

1.064096	5.790195	0.004665

1.060994	5.795409	0.003584

1.057909	5.796796	0.001077

1.054841	5.794337	0.002774

1.051791	5.794943	0.002760

1.048758	5.780754	0.002586

1.045741	5.779815	0.001634

1.042742	5.789203	0.010586

1.039759	5.772669	0.002696

1.036792	5.763944	0.000008

1.033842	5.776329	0.002109

1.030908	5.766442	0.007208

1.027990	5.765135	0.009174

1.025088	5.753613	0.000655

1.022202	5.761027	0.001015

1.019331	5.759674	0.010327

1.016477	5.760329	0.006349

1.013637	5.751645	0.003537

1.010813	5.753087	0.008606

1.008005	5.750217	0.012054

1.005211	5.736544	-0.005759

1.002432	5.752508	0.018067

0.999669	5.740512	0.010103

0.996920	5.744132	0.019803

0.994185	5.729600	-0.007099

0.991465	5.724788	0.001275

0.988760	5.719687	0.012512

0.986069	5.719091	0.000966

0.983392	5.724684	0.000642

0.980729	5.721117	-0.001981

0.978081	5.717862	-0.009440

0.975446	5.705539	0.002422

0.972825	5.713273	0.003575

0.970217	5.707818	0.001044

0.967623	5.709444	0.002402

0.965043	5.705596	-0.001871

0.962476	5.697715	0.011619

0.959922	5.693219	0.002359

0.957382	5.698532	-0.012050

0.954855	5.687427	0.010732

0.952340	5.681485	-0.000306

0.949839	5.688536	0.003463

0.947350	5.700367	0.044368

0.944874	5.695356	-0.028772

0.942410	5.685585	-0.018026

0.939959	5.686631	-0.007439

0.937521	5.670631	0.015645

0.935095	5.662748	0.012053

0.932681	5.671116	0.022692

0.930279	5.664007	0.006943

0.927889	5.661904	-0.001919

0.925512	5.637603	0.006167

0.923146	5.657563	-0.005137

0.920792	5.652642	0.014920

0.918449	5.650094	-0.010758

0.916119	5.660509	-0.021653

0.913800	5.633854	-0.003297

0.911492	5.656672	-0.018537

0.909196	5.645990	0.011544

0.906911	5.651987	-0.012967

0.904637	5.642030	0.015100

0.902375	5.652443	0.006211

0.900123	5.652515	0.005395

0.897883	5.658547	-0.030190

0.895653	5.640375	-0.010265

0.893435	5.650496	-0.009385

0.891227	5.650045	-0.008555

0.889030	5.615734	0.018820

0.886843	5.567720	-0.001323

0.884667	5.630657	0.005164

0.882502	5.647098	0.001816

0.880347	5.616141	0.015128

0.878202	5.605932	0.006475

0.876067	5.622863	0.016122

0.873943	5.608777	0.025405

0.871829	5.611328	-0.006654

0.869725	5.625059	0.002810

0.867630	5.634499	0.002131

0.865546	5.587843	-0.001612

0.863472	5.577419	0.002396

0.861407	5.611365	0.033762

0.859352	5.613290	-0.012450

0.857307	5.605087	-0.011340

0.855272	5.634795	-0.002341

0.853245	5.574258	0.005361

0.851229	5.567387	0.031907

0.849222	5.602667	-0.004541

0.847224	5.576580	0.014400

0.845235	5.570664	-0.014208

0.843256	5.593117	-0.000227

0.841285	5.606170	0.015386

0.839324	5.581075	0.027946

0.837372	5.578513	-0.013915

0.835429	5.641677	0.010282

0.833495	5.565129	0.018830

0.831570	5.553902	0.012278

0.829653	5.531057	-0.032990

0.827745	5.579798	0.043512

0.825846	5.589197	0.038284

0.823956	5.629754	0.032871

0.822074	5.544829	-0.017198

0.820200	5.530285	-0.011463

0.818335	5.525349	0.038497

0.816479	5.559286	-0.033504

0.814631	5.519784	0.022632

0.812791	5.545180	0.020427

0.810959	5.519048	-0.044270

0.809136	5.583788	0.009480

0.807321	5.574306	0.022158

0.805514	5.592592	0.054186

0.803715	5.541156	-0.024464

0.801923	5.484615	0.029320

0.800140	5.580802	0.027023

0.798365	5.532775	-0.017674

0.796598	5.621838	0.112094

0.794838	5.507706	0.033453

0.793086	5.470077	0.019709

0.791342	5.526596	0.036452

0.789605	5.531722	-0.007186

0.787876	5.569367	0.059493

0.786155	5.622277	0.070333

0.784441	5.556141	0.075072

0.782735	5.468820	-0.037831

0.781036	5.605829	0.105003

0.779344	5.445169	-0.039632

0.777660	5.496479	0.043634

0.775983	5.526795	0.019596

0.774313	5.496922	-0.016808

0.772651	5.533419	0.062146

0.770995	5.531681	0.018008

0.769347	5.499699	0.041055

0.767706	5.511269	0.053670

0.766072	5.501835	0.032794

0.764444	5.434006	-0.092019

0.762824	5.459411	-0.001317

0.761211	5.469284	0.010638

0.759604	5.556440	0.102863

0.758004	5.480069	-0.042443

0.756411	5.423576	-0.080697

0.754825	5.589554	0.164479

0.753246	5.476253	0.053751

0.751673	5.590577	0.150456

0.750107	5.427486	-0.101628

0.748547	5.538360	0.148318

0.746994	5.657848	0.198665

0.745447	5.468188	-0.019864

0.743907	5.503419	0.102740

0.742373	5.533844	0.073477

0.740846	5.447865	-0.019720

0.739325	5.484977	0.069919

0.737810	5.459083	0.211768

0.736301	5.517398	0.108693

0.734799	5.417260	0.098431

- ε for FA0.8Cs0.2PbI3 vs photon energy (eV)

Photon Energy (eV)	ε1	ε2

5.886830	1.924474	3.072659

5.842581	2.019819	3.075384

5.798990	2.068394	3.103435

5.756044	2.120704	3.081442

5.713730	2.186003	3.042467

5.672031	2.233378	2.992193

5.630938	2.251472	2.945732

5.590435	2.290540	2.895935

5.550508	2.327020	2.824524

5.511149	2.351618	2.738834

5.472343	2.378357	2.729074

5.434079	2.345870	2.636073

5.396346	2.344599	2.610754

5.359134	2.329864	2.582855

5.322429	2.294509	2.536571

5.286224	2.293454	2.522418

5.250508	2.258871	2.488601

5.215272	2.233727	2.460575

5.180504	2.207638	2.456037

5.146196	2.166691	2.469589

5.112340	2.139776	2.460175

5.078925	2.100475	2.457260

5.045945	2.069425	2.454255

5.013389	2.051621	2.481784

4.981251	2.020184	2.509109

4.949521	1.999382	2.537956

4.918193	1.978282	2.568891

4.887259	1.963883	2.583504

4.856710	1.950473	2.618038

4.826542	1.945543	2.652378

4.796745	1.940061	2.689183

4.767314	1.944883	2.722015

4.738242	1.955266	2.742076

4.709521	1.972941	2.770860

4.681147	1.991609	2.797616

4.653112	2.011741	2.824546

4.625410	2.028453	2.833974

4.598037	2.046490	2.846997

4.570985	2.060188	2.857771

4.544249	2.074133	2.861646

4.517825	2.092795	2.862267

4.491704	2.103240	2.862365

4.465886	2.117433	2.857874

4.440361	2.122668	2.853458

4.415126	2.123883	2.851834

4.390176	2.117604	2.844637

4.365508	2.115088	2.837658

4.341113	2.113304	2.830512

4.316990	2.102897	2.827160

4.293134	2.088845	2.823498

4.269539	2.077141	2.829535

4.246203	2.059786	2.829673

4.223120	2.042377	2.836934

4.200286	2.021434	2.838243

4.177698	2.000027	2.847790

4.155352	1.978901	2.863864

4.133243	1.951301	2.871212

4.111368	1.927404	2.889785

4.089723	1.899355	2.903220

4.068305	1.871750	2.922855

4.047110	1.842433	2.955648

4.026134	1.816122	2.982789

4.005375	1.788761	3.011874

3.984829	1.753439	3.045836

3.964492	1.729129	3.075945

3.944361	1.699638	3.116237

3.924434	1.671569	3.155075

3.904708	1.640084	3.208231

3.885178	1.608928	3.253481

3.865843	1.584229	3.303787

3.846699	1.555955	3.364751

3.827744	1.534358	3.426922

3.808975	1.510023	3.493580

3.790389	1.493653	3.567314

3.771983	1.480298	3.641554

3.753756	1.467662	3.714184

3.735703	1.455957	3.791362

3.717823	1.447444	3.874026

3.700114	1.454180	3.957628

3.682572	1.462301	4.037901

3.665196	1.469603	4.124821

3.647983	1.482492	4.214193

3.630931	1.503036	4.303370

3.614038	1.524312	4.387434

3.597301	1.556507	4.474335

3.580719	1.587910	4.561871

3.564288	1.633457	4.655359

3.548008	1.675860	4.742156

3.531876	1.722924	4.826172

3.515889	1.774338	4.914733

3.500047	1.835058	5.001774

3.484347	1.887578	5.081718

3.468787	1.949260	5.159263

3.453366	2.017009	5.243193

3.438081	2.088407	5.317435

3.422931	2.173987	5.390989

3.407914	2.258339	5.463298

3.393028	2.351944	5.530481

3.378271	2.446687	5.598713

3.363643	2.548138	5.675381

3.349140	2.649696	5.730378

3.334762	2.748313	5.789727

3.320507	2.844445	5.844581

3.306374	2.944206	5.896604

3.292360	3.052646	5.941499

3.278465	3.164924	5.971684

3.264686	3.288122	6.007893

3.251023	3.419204	6.033539

3.237473	3.552167	6.044506

3.224037	3.684475	6.058282

3.210711	3.817847	6.055934

3.197495	3.944160	6.043244

3.184388	4.072829	6.029393

3.171387	4.195148	5.996727

3.158493	4.312154	5.976551

3.145703	4.418438	5.939744

3.133016	4.521049	5.896182

3.120431	4.624746	5.850690

3.107947	4.710546	5.804811

3.095562	4.800101	5.750417

3.083276	4.880143	5.705004

3.071087	4.961161	5.646663

3.058994	5.032495	5.587332

3.046996	5.106408	5.531141

3.035092	5.168794	5.469899

3.023281	5.232794	5.415325

3.011561	5.288115	5.348930

2.999932	5.346167	5.290550

2.988392	5.394430	5.226031

2.976941	5.450702	5.166006

2.965577	5.499428	5.104709

2.954300	5.537938	5.033648

2.943108	5.577671	4.975667

2.932001	5.615299	4.904657

2.920978	5.645179	4.846936

2.910037	5.674493	4.778178

2.899178	5.703388	4.708326

2.888400	5.713746	4.649835

2.877702	5.728884	4.582805

2.867082	5.735064	4.525287

2.856541	5.737455	4.462636

2.846077	5.734744	4.409968

2.835690	5.730861	4.363343

2.825378	5.718829	4.318185

2.815142	5.706368	4.282062

2.804979	5.699126	4.247316

2.794889	5.684490	4.218476

2.784872	5.673903	4.190084

2.774927	5.661234	4.175272

2.765052	5.646333	4.155278

2.755248	5.633359	4.145787

2.745512	5.627356	4.151136

2.735846	5.620642	4.140128

2.726248	5.614864	4.142664

2.716716	5.608051	4.143474

2.707252	5.617451	4.154770

2.697853	5.613663	4.160604

2.688519	5.614461	4.180588

2.679250	5.626816	4.191264

2.670044	5.637309	4.205390

2.660902	5.656563	4.222516

2.651822	5.679461	4.242366

2.642804	5.702122	4.254560

2.633847	5.729533	4.267752

2.624951	5.759804	4.290164

2.616115	5.793910	4.302367

2.607338	5.832039	4.315989

2.598620	5.876311	4.329023

2.589961	5.919868	4.348515

2.581358	5.970502	4.360526

2.572814	6.019327	4.369017

2.564325	6.069950	4.371165

2.555892	6.128205	4.369030

2.547515	6.187822	4.366157

2.539193	6.250373	4.357909

2.530925	6.307471	4.351149

2.522711	6.375746	4.341879

2.514550	6.428193	4.324900

2.506442	6.495228	4.297736

2.498386	6.566185	4.284470

2.490382	6.625752	4.244120

2.482429	6.683105	4.198650

2.474527	6.732966	4.172230

2.466675	6.786798	4.129351

2.458873	6.835859	4.081615

2.451120	6.884920	4.033202

2.443417	6.934113	3.987669

2.435761	6.976871	3.936687

2.428154	7.015507	3.884766

2.420594	7.052605	3.837045

2.413081	7.088882	3.785321

2.405614	7.119088	3.735759

2.398194	7.147109	3.679489

2.390820	7.178138	3.627617

2.383491	7.207741	3.574460

2.376207	7.237175	3.520435

2.368967	7.255526	3.466114

2.361772	7.275590	3.411319

2.354620	7.292567	3.361545

2.347511	7.313138	3.304438

2.340446	7.328070	3.256294

2.333423	7.338193	3.206111

2.326442	7.354021	3.153700

2.319503	7.357846	3.103161

2.312605	7.369286	3.051555

2.305749	7.373168	2.998452

2.298933	7.379854	2.949507

2.292157	7.385378	2.901643

2.285422	7.384399	2.856275

2.278726	7.386890	2.803078

2.272069	7.386437	2.758604

2.265451	7.382604	2.717130

2.258872	7.380621	2.674190

2.252331	7.378905	2.633768

2.245827	7.370442	2.586888

2.239362	7.369224	2.545879

2.232934	7.367050	2.503314

2.226542	7.353192	2.466029

2.220187	7.353256	2.424984

2.213869	7.343346	2.388761

2.207587	7.334994	2.348797

2.201340	7.330778	2.313666

2.195129	7.323399	2.280900

2.188952	7.309884	2.248135

2.182811	7.303961	2.214883

2.176704	7.296515	2.184505

2.170631	7.285475	2.152784

2.164593	7.273106	2.123007

2.158587	7.265657	2.089435

2.152616	7.253895	2.060529

2.146677	7.240789	2.032261

2.140771	7.237845	2.005196

2.134898	7.224135	1.974853

2.129057	7.214119	1.951659

2.123248	7.202539	1.920230

2.117471	7.190275	1.896470

2.111725	7.184896	1.870542

2.106011	7.174134	1.846545

2.100327	7.159523	1.824190

2.094674	7.148790	1.801396

2.089052	7.138115	1.775252

2.083460	7.128561	1.757120

2.077898	7.117192	1.736202

2.072366	7.107475	1.713835

2.066863	7.091058	1.695284

2.061389	7.078861	1.671003

2.055945	7.068927	1.650593

2.050529	7.055442	1.626153

2.045143	7.050879	1.617092

2.039784	7.035703	1.599131

2.034454	7.027332	1.578610

2.029151	7.007605	1.552168

2.023876	6.992740	1.526211

2.018629	6.981452	1.520988

2.013409	6.977590	1.506392

2.008216	6.947866	1.489543

2.003050	6.944290	1.472610

1.997911	6.925851	1.444299

1.992798	6.911968	1.473367

1.987711	6.894949	1.468779

1.982651	6.893078	1.475904

1.977616	6.936777	1.442992

1.972607	6.912635	1.418324

1.967623	6.908748	1.363958

1.962664	6.894464	1.369277

1.957731	6.876138	1.352364

1.952823	6.868448	1.345465

1.947939	6.857748	1.329437

1.943080	6.850199	1.315041

1.938245	6.840539	1.308314

1.933434	6.829872	1.291333

1.928647	6.827347	1.278846

1.923884	6.809227	1.282856

1.919145	6.804193	1.262616

1.914429	6.799678	1.246374

1.909737	6.787875	1.237644

1.905067	6.780140	1.230846

1.900420	6.773698	1.218184

1.895796	6.766163	1.208918

1.891195	6.756915	1.197154

1.886616	6.748401	1.190732

1.882060	6.739178	1.181603

1.877525	6.732672	1.172640

1.873013	6.726114	1.161892

1.868522	6.721512	1.150183

1.864053	6.711508	1.142454

1.859605	6.704996	1.135895

1.855179	6.697794	1.129068

1.850774	6.692732	1.118722

1.846390	6.687221	1.110821

1.842026	6.679338	1.103233

1.837684	6.674483	1.096893

1.833362	6.667358	1.090494

1.829061	6.663052	1.082654

1.824779	6.657319	1.075815

1.820518	6.648369	1.068267

1.816277	6.644134	1.059065

1.812056	6.639266	1.055862

1.807855	6.633570	1.048553

1.803673	6.628422	1.042822

1.799510	6.620744	1.036943

1.795367	6.620525	1.031035

1.791243	6.617398	1.024258

1.787138	6.610414	1.019336

1.783052	6.602129	1.014590

1.778985	6.599097	1.007698

1.774937	6.595261	1.001277

1.770907	6.594324	0.996816

1.766895	6.591957	0.990761

1.762902	6.587693	0.988727

1.758927	6.584601	0.982874

1.754970	6.584290	0.979028

1.751030	6.581935	0.973636

1.747109	6.576436	0.967667

1.743205	6.575043	0.963264

1.739319	6.572188	0.959645

1.735450	6.571915	0.954551

1.731599	6.569652	0.950919

1.727765	6.566825	0.946479

1.723948	6.567093	0.944237

1.720148	6.565377	0.940135

1.716365	6.563522	0.935461

1.712598	6.561658	0.932463

1.708848	6.560976	0.929888

1.705115	6.560218	0.925541

1.701398	6.561210	0.922306

1.697697	6.560913	0.920093

1.694013	6.564518	0.917802

1.690345	6.566256	0.913897

1.686693	6.570895	0.911290

1.683056	6.570128	0.908005

1.679436	6.576043	0.906453

1.675831	6.577964	0.903723

1.672242	6.583610	0.901165

1.668668	6.591143	0.899777

1.665109	6.595800	0.896632

1.661566	6.602052	0.891978

1.658038	6.612569	0.891252

1.654526	6.620659	0.887687

1.651028	6.631536	0.884747

1.647545	6.641843	0.879391

1.644077	6.655725	0.874083

1.640624	6.669883	0.868825

1.637185	6.686692	0.862068

1.633761	6.704136	0.851975

1.630351	6.720516	0.840280

1.626956	6.742768	0.827911

1.623574	6.761802	0.811613

1.620207	6.781746	0.796662

1.616855	6.802262	0.782639

1.613516	6.822573	0.760729

1.610191	6.841821	0.732125

1.606880	6.860560	0.700673

1.603582	6.876478	0.667896

1.600299	6.888453	0.628596

1.597028	6.899220	0.592662

1.593772	6.904342	0.551693

1.590528	6.907182	0.509935

1.587298	6.904983	0.465698

1.584082	6.898046	0.423532

1.580878	6.886145	0.381196

1.577688	6.870610	0.341433

1.574510	6.848907	0.300590

1.571346	6.828892	0.265303

1.568194	6.812226	0.235717

1.565055	6.792783	0.209992

1.561929	6.762383	0.184267

1.558815	6.729803	0.161182

1.555714	6.697296	0.135799

1.552625	6.673554	0.117666

1.549549	6.652316	0.105027

1.546485	6.621207	0.093736

1.543433	6.593317	0.083343

1.540394	6.564559	0.073920

1.537367	6.538359	0.063593

1.534351	6.513027	0.055198

1.531348	6.490458	0.049124

1.528356	6.466369	0.046435

1.525376	6.442485	0.043684

1.522408	6.422056	0.037359

1.519452	6.397828	0.036292

1.516507	6.374632	0.033085

1.513574	6.349623	0.028553

1.510652	6.328158	0.023188

1.507742	6.324907	0.019525

1.504843	6.331679	0.014951

1.501955	6.337678	0.012566

1.499079	6.330634	0.013262

1.496213	6.315516	0.013392

1.493359	6.311179	0.013453

1.490516	6.300862	0.015109

1.487683	6.271831	0.017793

1.484862	6.254765	0.018662

1.482051	6.255575	0.017159

1.479252	6.253855	0.017919

1.476462	6.234321	0.021675

1.473684	6.217293	0.022470

1.470916	6.216412	0.024014

1.468159	6.212330	0.023415

1.465412	6.201718	0.028031

1.462675	6.185198	0.035067

1.459949	6.165763	0.036802

1.457233	6.154685	0.039432

1.454528	6.138942	0.038944

1.451832	6.125364	0.041941

1.449147	6.111130	0.041244

1.446472	6.101779	0.040602

1.443806	6.090802	0.041646

1.441151	6.078314	0.039480

1.438506	6.070057	0.043192

1.435870	6.058450	0.041634

1.433244	6.048271	0.040627

1.430628	6.039827	0.039825

1.428022	6.035060	0.040184

1.425425	6.025255	0.039568

1.422838	6.015310	0.039293

1.420260	6.010249	0.039226

1.417692	6.004498	0.038686

1.415133	5.996378	0.039287

1.412584	5.984643	0.037778

1.410044	5.974809	0.036295

1.407513	5.974650	0.033730

1.404991	5.982339	0.032210

1.402479	5.993640	0.030665

1.399975	6.002005	0.032393

1.397481	6.001910	0.033464

1.394996	5.991245	0.034663

1.392519	5.978376	0.036568

1.390052	5.964139	0.039452

1.387594	5.946204	0.039280

1.385144	5.940765	0.035619

1.382703	5.944746	0.035511

1.380271	5.948042	0.035555

1.377847	5.944876	0.037437

1.375432	5.930125	0.040484

1.373026	5.912539	0.039967

1.370628	5.904704	0.038212

1.368239	5.909504	0.037717

1.365858	5.917717	0.038520

1.363486	5.917949	0.040265

1.361122	5.905196	0.041529

1.358766	5.881397	0.041948

1.356419	5.866824	0.040476

1.354080	5.862806	0.038898

1.351749	5.867738	0.038033

1.349426	5.874167	0.037483

1.347111	5.879234	0.038175

1.344805	5.880836	0.039811

1.342506	5.878460	0.039671

1.340216	5.875183	0.043219

1.337933	5.870234	0.042967

1.335658	5.864247	0.043078

1.333391	5.855813	0.044924

1.331132	5.845344	0.046135

1.328881	5.837420	0.044672

1.326638	5.830287	0.044943

1.324402	5.817271	0.046640

1.322173	5.811851	0.042617

1.319953	5.809739	0.044445

1.317740	5.807937	0.042717

1.315535	5.803602	0.043276

1.313337	5.797923	0.044277

1.311146	5.795035	0.043257

1.308963	5.787367	0.042836

1.306788	5.777975	0.043529

1.304619	5.775063	0.041006

1.302459	5.773733	0.044403

1.300305	5.772931	0.044610

1.298159	5.770387	0.042655

1.296019	5.769996	0.043603

1.293887	5.768326	0.043344

1.291763	5.761366	0.042980

1.289645	5.753072	0.048938

1.287534	5.742955	0.050983

1.285431	5.733360	0.045030

1.283334	5.724989	0.050965

1.281244	5.718343	0.042985

1.279162	5.713917	0.041752

1.277086	5.708218	0.046561

1.275017	5.703781	0.043561

1.272955	5.700144	0.042111

1.270900	5.692409	0.043622

1.268851	5.685757	0.040901

1.266809	5.688364	0.038714

1.264774	5.698008	0.039805

1.262746	5.704830	0.040565

1.260724	5.708699	0.039094

1.258709	5.715441	0.039561

1.256700	5.710030	0.039583

1.254698	5.696165	0.041060

1.252702	5.684851	0.040140

1.250713	5.679521	0.039836

1.248730	5.680455	0.039220

1.246754	5.684220	0.038932

1.244784	5.692870	0.037444

1.242821	5.699441	0.037287

1.240863	5.705186	0.040044

1.224385	5.565575	0.040686

1.220322	5.559224	0.042082

1.216285	5.545697	0.039829

1.212273	5.544676	0.045780

1.208287	5.538555	0.043189

1.204326	5.534178	0.042817

1.200390	5.528696	0.042945

1.196478	5.518814	0.042824

1.192591	5.514611	0.044124

1.188727	5.509287	0.040404

1.184888	5.505142	0.041452

1.181073	5.508374	0.041136

1.177281	5.499308	0.042593

1.173512	5.497798	0.045697

1.169767	5.487724	0.044215

1.166045	5.485492	0.042867

1.162345	5.480720	0.042676

1.158667	5.478758	0.043031

1.155012	5.467474	0.045530

1.151380	5.464995	0.045455

1.147769	5.469355	0.041573

1.144179	5.464729	0.044278

1.140612	5.460574	0.041543

1.137066	5.454755	0.045381

1.133540	5.447044	0.043888

1.130036	5.446937	0.044401

1.126553	5.435376	0.045370

1.123090	5.436106	0.043189

1.119648	5.438709	0.044336

1.116226	5.435937	0.043004

1.112824	5.429062	0.042484

1.109442	5.425740	0.043813

1.106080	5.418962	0.044094

1.102737	5.416675	0.042803

1.099414	5.410303	0.043708

1.096110	5.413889	0.047418

1.092825	5.406080	0.045660

1.089559	5.409255	0.050191

1.086312	5.398592	0.045735

1.083084	5.397423	0.044885

1.079874	5.395901	0.052526

1.076682	5.389208	0.043052

1.073509	5.383592	0.045829

1.070353	5.384069	0.042947

1.067216	5.375639	0.044675

1.064096	5.368670	0.044965

1.060994	5.368106	0.043727

1.057909	5.372458	0.039364

1.054841	5.369904	0.041205

1.051791	5.366240	0.042779

1.048758	5.362624	0.039809

1.045741	5.359655	0.041409

1.042742	5.356123	0.036563

1.039759	5.350958	0.037649

1.036792	5.348869	0.039571

1.033842	5.346883	0.043954

1.030908	5.340505	0.037189

1.027990	5.341812	0.031975

1.025088	5.333179	0.044203

1.022202	5.334514	0.040741

1.019331	5.324972	0.040130

1.016477	5.324403	0.042181

1.013637	5.323379	0.039633

1.010813	5.325588	0.035196

1.008005	5.316624	0.035407

1.005211	5.315239	0.029139

1.002432	5.311218	0.037302

0.999669	5.313823	0.033462

0.996920	5.303802	0.039445

0.994185	5.312386	0.029636

0.991465	5.304667	0.029964

0.988760	5.290511	0.035975

0.986069	5.297513	0.033607

0.983392	5.301748	0.029591

0.980729	5.300524	0.029516

0.978081	5.300256	0.029693

0.975446	5.292055	0.030562

0.972825	5.289063	0.036661

0.970217	5.275868	0.029853

0.967623	5.294326	0.035588

0.965043	5.277583	0.033756

0.962476	5.294487	0.028103

0.959922	5.269241	0.031082

0.957382	5.292152	0.026707

0.954855	5.265224	0.031424

0.952340	5.275768	0.029062

0.949839	5.268915	0.034134

0.947350	5.275227	0.021565

0.944874	5.250683	0.035963

0.942410	5.255314	0.031857

0.939959	5.279493	0.024222

0.937521	5.268815	0.032274

0.935095	5.263988	0.028291

0.932681	5.249855	0.032257

0.930279	5.256833	0.017541

0.927889	5.257511	0.011263

0.925512	5.265007	0.036263

0.923146	5.249409	0.021392

0.920792	5.240851	0.023434

0.918449	5.243863	0.014765

0.916119	5.244755	0.031754

0.913800	5.234289	0.020316

0.911492	5.253265	0.026805

0.909196	5.250329	0.020081

0.906911	5.257909	0.033185

0.904637	5.220079	0.015173

0.902375	5.230413	0.016928

0.900123	5.238332	0.026457

0.897883	5.225634	0.009354

0.895653	5.233767	0.016222

0.893435	5.213599	0.022562

0.891227	5.224540	0.008463

0.889030	5.233497	0.028610

0.886843	5.209611	0.010622

0.884667	5.225565	0.025005

0.882502	5.220892	0.026980

0.880347	5.240338	0.029724

0.878202	5.206687	0.016207

0.876067	5.223556	0.033693

0.873943	5.224790	0.029583

0.871829	5.219201	0.021316

0.869725	5.213685	0.010265

0.867630	5.227026	0.032680

0.865546	5.206340	0.017956

0.863472	5.235427	0.029036

0.861407	5.213751	0.020611

0.859352	5.221486	0.017785

0.857307	5.232618	0.042172

0.855272	5.210132	0.020265

0.853245	5.218227	0.025531

0.851229	5.190765	0.009416

0.849222	5.212831	0.026003

0.847224	5.206713	0.044416

0.845235	5.206766	0.009572

0.843256	5.213373	0.018425

0.841285	5.207481	0.012173

0.839324	5.219122	0.042290

0.837372	5.207203	0.010817

0.835429	5.204528	0.020805

0.833495	5.217882	0.051102

0.831570	5.202735	0.009416

0.829653	5.210767	0.031592

0.827745	5.197524	0.010383

0.825846	5.197210	0.027803

0.823956	5.198013	0.014932

0.822074	5.186255	0.021083

0.820200	5.189106	0.003908

0.818335	5.193542	0.030337

0.816479	5.180336	0.011005

0.814631	5.201397	0.016001

0.812791	5.177384	0.000864

0.810959	5.194953	0.018677

0.809136	5.190260	0.032931

0.807321	5.188551	0.027136

0.805514	5.197194	0.037965

0.803715	5.191859	0.024761

0.801923	5.198895	0.047837

0.800140	5.201342	0.021873

0.798365	5.177126	0.030168

0.796598	5.175199	0.010658

0.794838	5.195554	0.068112

0.793086	5.196743	0.056185

0.791342	5.175741	0.010308

0.789605	5.178576	0.007674

0.787876	5.181663	0.053734

0.786155	5.188229	0.055657

0.784441	5.188715	0.064253

0.782735	5.176486	0.019928

0.781036	5.176747	0.036427

0.779344	5.171615	0.021334

0.777660	5.171559	0.034217

0.775983	5.176556	0.037409

0.774313	5.177302	0.048473

0.772651	5.181040	0.029550

0.770995	5.169463	0.030882

0.769347	5.169824	0.043873

0.767706	5.159020	0.021822

0.766072	5.156933	0.023715

0.764444	5.167052	0.080572

0.762824	5.169236	0.033924

0.761211	5.153802	0.012848

0.759604	5.171052	0.042448

0.758004	5.156634	0.038647

0.756411	5.162848	0.031690

0.754825	5.158353	0.066843

0.753246	5.161063	0.065155

0.751673	5.148812	0.048609

0.750107	5.157721	0.014019

0.748547	5.144656	0.028026

0.746994	5.155300	0.024513

0.745447	5.152995	0.070013

0.743907	5.156818	0.043915

0.742373	5.146018	0.027198

0.740846	5.158388	0.076452

0.739325	5.155150	0.016882

0.737810	5.160272	0.064720

0.736301	5.150866	0.069304

0.734799	5.152742	0.056679

- ε for FA0.7Cs0.3PbI3 vs. photon energy (eV)

Photon Energy (eV)	ε1	ε2

5.886830	1.827677	2.588772

5.842581	1.818874	2.593727

5.798990	1.936103	2.753106

5.756044	1.995517	2.547726

5.713730	2.007493	2.619824

5.672031	2.035501	2.432681

5.630938	2.108345	2.509121

5.590435	2.092424	2.366244

5.550508	2.163907	2.376870

5.511149	2.175212	2.352131

5.472343	2.153591	2.312477

5.434079	2.108896	2.262631

5.396346	2.132443	2.228216

5.359134	2.117088	2.183005

5.322429	2.076489	2.151150

5.286224	2.034837	2.168425

5.250508	2.010152	2.119915

5.215272	1.985588	2.093427

5.180504	1.952812	2.136116

5.146196	1.892484	2.103582

5.112340	1.863491	2.126173

5.078925	1.857189	2.114012

5.045945	1.819445	2.136948

5.013389	1.801569	2.177586

4.981251	1.780071	2.197662

4.949521	1.745403	2.216317

4.918193	1.716623	2.250961

4.887259	1.721977	2.287662

4.856710	1.698049	2.315084

4.826542	1.701583	2.354051

4.796745	1.711758	2.385998

4.767314	1.722606	2.439871

4.738242	1.737104	2.457386

4.709521	1.737568	2.491685

4.681147	1.758535	2.520964

4.653112	1.776897	2.535812

4.625410	1.802080	2.554046

4.598037	1.794481	2.555729

4.570985	1.816315	2.551908

4.544249	1.821309	2.566217

4.517825	1.838861	2.564403

4.491704	1.855047	2.559813

4.465886	1.862283	2.546755

4.440361	1.875260	2.568660

4.415126	1.870119	2.564951

4.390176	1.839361	2.557444

4.365508	1.861218	2.578184

4.341113	1.850895	2.548754

4.316990	1.841298	2.568252

4.293134	1.839124	2.564171

4.269539	1.818359	2.554862

4.246203	1.807637	2.554496

4.223120	1.785711	2.581561

4.200286	1.772482	2.579545

4.177698	1.751376	2.617376

4.155352	1.728407	2.600947

4.133243	1.704849	2.619900

4.111368	1.674269	2.638722

4.089723	1.656418	2.664920

4.068305	1.620197	2.685741

4.047110	1.611827	2.716604

4.026134	1.577827	2.749413

4.005375	1.551453	2.781880

3.984829	1.521516	2.800575

3.964492	1.488773	2.836619

3.944361	1.471684	2.867964

3.924434	1.431756	2.920151

3.904708	1.411950	2.982327

3.885178	1.390241	3.007672

3.865843	1.361745	3.078226

3.846699	1.341613	3.127462

3.827744	1.315357	3.193209

3.808975	1.311285	3.246839

3.790389	1.296506	3.322718

3.771983	1.286181	3.381634

3.753756	1.274981	3.458536

3.735703	1.262595	3.531123

3.717823	1.269935	3.612374

3.700114	1.279413	3.664978

3.682572	1.288748	3.759543

3.665196	1.290516	3.853913

3.647983	1.313973	3.928921

3.630931	1.337843	4.000145

3.614038	1.358053	4.090464

3.597301	1.385482	4.158367

3.580719	1.407917	4.258561

3.564288	1.449957	4.337129

3.548008	1.503184	4.412611

3.531876	1.555439	4.490401

3.515889	1.588073	4.561016

3.500047	1.648886	4.654766

3.484347	1.724810	4.728762

3.468787	1.774278	4.789861

3.453366	1.832659	4.860226

3.438081	1.900063	4.944312

3.422931	1.976923	5.012600

3.407914	2.064903	5.079313

3.393028	2.170710	5.124480

3.378271	2.260683	5.211406

3.363643	2.363810	5.248642

3.349140	2.450484	5.329594

3.334762	2.553360	5.351972

3.320507	2.639809	5.393610

3.306374	2.733530	5.440732

3.292360	2.873831	5.458747

3.278465	2.953076	5.474915

3.264686	3.083986	5.508902

3.251023	3.206719	5.503704

3.237473	3.327022	5.507417

3.224037	3.454004	5.490604

3.210711	3.537671	5.471056

3.197495	3.663854	5.458053

3.184388	3.773070	5.411025

3.171387	3.863126	5.362032

3.158493	3.921580	5.325601

3.145703	4.025731	5.302650

3.133016	4.092821	5.250138

3.120431	4.173647	5.206436

3.107947	4.238075	5.149200

3.095562	4.257722	5.101248

3.083276	4.334310	5.058609

3.071087	4.366525	5.010674

3.058994	4.389082	4.958962

3.046996	4.442053	4.917221

3.035092	4.486898	4.887088

3.023281	4.524543	4.862321

3.011561	4.549265	4.823332

2.999932	4.587577	4.785045

2.988392	4.642999	4.761776

2.976941	4.666821	4.742892

2.965577	4.722447	4.675016

2.954300	4.774121	4.641758

2.943108	4.827978	4.622184

2.932001	4.835596	4.554953

2.920978	4.884379	4.482962

2.910037	4.890099	4.468034

2.899178	4.930953	4.420723

2.888400	4.964566	4.374023

2.877702	4.974320	4.317763

2.867082	4.972954	4.256297

2.856541	4.998196	4.211618

2.846077	4.981503	4.174048

2.835690	4.969967	4.115085

2.825378	4.975685	4.096072

2.815142	4.958999	4.084790

2.804979	4.958997	4.054309

2.794889	4.945392	4.038366

2.784872	4.922151	4.035717

2.774927	4.928017	4.015196

2.765052	4.916782	4.020152

2.755248	4.905756	3.999438

2.745512	4.888688	4.038807

2.735846	4.907619	4.019270

2.726248	4.902113	4.019800

2.716716	4.907816	4.054677

2.707252	4.917225	4.063933

2.697853	4.917203	4.071873

2.688519	4.925748	4.097194

2.679250	4.954181	4.121918

2.670044	4.977327	4.153341

2.660902	5.008238	4.158496

2.651822	5.021903	4.184327

2.642804	5.066376	4.216020

2.633847	5.112723	4.220549

2.624951	5.134046	4.253358

2.616115	5.181676	4.250531

2.607338	5.229307	4.274882

2.598620	5.285040	4.278488

2.589961	5.334812	4.286325

2.581358	5.394144	4.291878

2.572814	5.436744	4.286894

2.564325	5.494958	4.287358

2.555892	5.558943	4.294704

2.547515	5.614931	4.260543

2.539193	5.660847	4.267538

2.530925	5.721337	4.251198

2.522711	5.778995	4.219195

2.514550	5.848691	4.211273

2.506442	5.896181	4.167258

2.498386	5.947466	4.133165

2.490382	5.992589	4.122225

2.482429	6.066504	4.080120

2.474527	6.080755	4.049984

2.466675	6.126152	4.010976

2.458873	6.202669	3.983785

2.451120	6.217896	3.943426

2.443417	6.267810	3.884965

2.435761	6.293411	3.832331

2.428154	6.336761	3.806056

2.420594	6.370816	3.747149

2.413081	6.414819	3.716865

2.405614	6.425762	3.629789

2.398194	6.470211	3.611300

2.390820	6.477419	3.545413

2.383491	6.494493	3.523015

2.376207	6.512587	3.454994

2.368967	6.521040	3.403348

2.361772	6.560776	3.375252

2.354620	6.580710	3.318892

2.347511	6.576750	3.273749

2.340446	6.576822	3.225612

2.333423	6.595275	3.184107

2.326442	6.611494	3.125319

2.319503	6.627619	3.113709

2.312605	6.634273	3.069412

2.305749	6.618480	3.011132

2.298933	6.642982	2.973640

2.292157	6.647022	2.928542

2.285422	6.651163	2.904515

2.278726	6.607977	2.838332

2.272069	6.642237	2.818316

2.265451	6.637123	2.779283

2.258872	6.639629	2.744385

2.252331	6.622838	2.712873

2.245827	6.606306	2.671014

2.239362	6.613647	2.642460

2.232934	6.606264	2.600584

2.226542	6.577826	2.554065

2.220187	6.580314	2.543945

2.213869	6.576454	2.519032

2.207587	6.581192	2.481708

2.201340	6.555707	2.465521

2.195129	6.558434	2.439877

2.188952	6.527100	2.413442

2.182811	6.550406	2.383204

2.176704	6.512787	2.378776

2.170631	6.515771	2.352742

2.164593	6.507424	2.334844

2.158587	6.493248	2.313350

2.152616	6.503262	2.296733

2.146677	6.502357	2.298029

2.140771	6.491144	2.279693

2.134898	6.485799	2.275825

2.129057	6.480946	2.272979

2.123248	6.469388	2.241182

2.117471	6.479871	2.223105

2.111725	6.483277	2.220988

2.106011	6.488372	2.203958

2.100327	6.482753	2.178774

2.094674	6.527488	2.181942

2.089052	6.513424	2.150598

2.083460	6.521754	2.128026

2.077898	6.531587	2.120732

2.072366	6.563168	2.124677

2.066863	6.549807	2.073566

2.061389	6.587194	2.046547

2.055945	6.521248	2.011094

2.050529	6.545990	2.000731

2.045143	6.548976	1.960692

2.039784	6.572579	1.934850

2.034454	6.524408	1.913140

2.029151	6.537159	1.892953

2.023876	6.541025	1.862717

2.018629	6.504262	1.833213

2.013409	6.557713	1.816910

2.008216	6.520899	1.783226

2.003050	6.516936	1.770346

1.997911	6.495773	1.743352

1.992798	6.485091	1.712062

1.987711	6.491994	1.701313

1.982651	6.456525	1.671403

1.977616	6.448296	1.640391

1.972607	6.447924	1.622822

1.967623	6.442122	1.608726

1.962664	6.442088	1.601458

1.957731	6.429519	1.586046

1.952823	6.397419	1.559961

1.947939	6.383548	1.539501

1.943080	6.385305	1.538842

1.938245	6.371264	1.513344

1.933434	6.354780	1.502914

1.928647	6.338884	1.476361

1.923884	6.330672	1.477539

1.919145	6.319502	1.463931

1.914429	6.303127	1.438908

1.909737	6.300908	1.433913

1.905067	6.298352	1.438353

1.900420	6.276242	1.421550

1.895796	6.264998	1.403811

1.891195	6.253442	1.401152

1.886616	6.218074	1.365922

1.882060	6.225867	1.374779

1.877525	6.212090	1.365528

1.873013	6.199872	1.353405

1.868522	6.188260	1.355420

1.864053	6.174846	1.333903

1.859605	6.163364	1.323853

1.855179	6.143472	1.320649

1.850774	6.127648	1.309880

1.846390	6.122424	1.316642

1.842026	6.089710	1.282318

1.837684	6.083046	1.261759

1.833362	6.049958	1.268103

1.829061	6.037066	1.255611

1.824779	6.024432	1.265351

1.820518	5.997934	1.249673

1.816277	5.966803	1.239053

1.812056	5.941606	1.236333

1.807855	5.913026	1.194279

1.803673	5.862955	1.153131

1.799510	5.832358	1.096364

1.795367	5.836934	1.032629

1.791243	5.860941	1.005396

1.787138	5.863022	0.965204

1.783052	5.865060	0.936716

1.778985	5.858779	0.903495

1.774937	5.888580	0.880387

1.770907	5.913621	0.857483

1.766895	5.914391	0.847756

1.762902	5.952824	0.817609

1.758927	5.980042	0.812340

1.754970	5.993862	0.806847

1.751030	5.967167	0.778865

1.747109	5.999362	0.775188

1.743205	6.016864	0.775881

1.739319	6.041507	0.770180

1.735450	6.057333	0.770374

1.731599	6.065966	0.754142

1.727765	6.077084	0.746496

1.723948	6.099515	0.761811

1.720148	6.114096	0.753895

1.716365	6.108707	0.746071

1.712598	6.116111	0.740648

1.708848	6.135469	0.754014

1.705115	6.159001	0.753220

1.701398	6.162775	0.754622

1.697697	6.186553	0.766703

1.694013	6.196210	0.757877

1.690345	6.212734	0.780487

1.686693	6.217594	0.764406

1.683056	6.216946	0.762656

1.679436	6.224539	0.762587

1.675831	6.230488	0.742090

1.672242	6.250985	0.784548

1.668668	6.257783	0.767132

1.665109	6.274636	0.767001

1.661566	6.272044	0.787581

1.658038	6.273062	0.768799

1.654526	6.291459	0.783971

1.651028	6.280594	0.752259

1.647545	6.292194	0.766102

1.644077	6.287564	0.756518

1.640624	6.298497	0.751383

1.637185	6.312581	0.749857

1.633761	6.314440	0.737778

1.630351	6.319407	0.749607

1.626956	6.322065	0.722320

1.623574	6.320998	0.727737

1.620207	6.341999	0.709061

1.616855	6.351582	0.710940

1.613516	6.362361	0.685280

1.610191	6.358429	0.657459

1.606880	6.370991	0.663759

1.603582	6.368569	0.626462

1.600299	6.374042	0.615514

1.597028	6.372607	0.571276

1.593772	6.370794	0.541858

1.590528	6.364872	0.519244

1.587298	6.351311	0.493376

1.584082	6.341856	0.456509

1.580878	6.333663	0.433512

1.577688	6.311033	0.414060

1.574510	6.287270	0.376922

1.571346	6.266885	0.356042

1.568194	6.250416	0.329781

1.565055	6.232668	0.315268

1.561929	6.205762	0.307293

1.558815	6.172783	0.293620

1.555714	6.146023	0.272113

1.552625	6.125249	0.266150

1.549549	6.104039	0.256780

1.546485	6.086687	0.243824

1.543433	6.058404	0.242473

1.540394	6.038953	0.230601

1.537367	6.011635	0.231337

1.534351	5.980578	0.232145

1.531348	5.965690	0.226915

1.528356	5.945549	0.229353

1.525376	5.929255	0.220158

1.522408	5.909404	0.220660

1.519452	5.890039	0.218111

1.516507	5.872413	0.214414

1.513574	5.849319	0.213116

1.510652	5.824380	0.211054

1.507742	5.818851	0.209378

1.504843	5.822388	0.208039

1.501955	5.826269	0.207591

1.499079	5.818170	0.208188

1.496213	5.803813	0.206422

1.493359	5.802357	0.204778

1.490516	5.792449	0.206090

1.487683	5.766886	0.206313

1.484862	5.752876	0.202782

1.482051	5.749558	0.201797

1.479252	5.749710	0.202386

1.476462	5.735930	0.201838

1.473684	5.717401	0.200042

1.470916	5.714563	0.199071

1.468159	5.715637	0.198031

1.465412	5.710460	0.203655

1.462675	5.699025	0.204428

1.459949	5.679709	0.199654

1.457233	5.671478	0.202114

1.454528	5.660546	0.202001

1.451832	5.641442	0.198042

1.449147	5.634959	0.199341

1.446472	5.621766	0.194455

1.443806	5.614818	0.197584

1.441151	5.599254	0.191711

1.438506	5.589534	0.185372

1.435870	5.577584	0.183772

1.433244	5.560338	0.175148

1.430628	5.549202	0.172801

1.428022	5.541916	0.163495

1.425425	5.533222	0.165052

1.422838	5.516595	0.153065

1.420260	5.507726	0.147237

1.417692	5.501720	0.144632

1.415133	5.486813	0.133578

1.412584	5.474427	0.125804

1.410044	5.460464	0.114747

1.407513	5.455647	0.105609

1.404991	5.460540	0.099700

1.402479	5.468736	0.094603

1.399975	5.474967	0.090634

1.397481	5.473444	0.088635

1.394996	5.459394	0.087482

1.392519	5.445741	0.083071

1.390052	5.426403	0.080289

1.387594	5.407440	0.072426

1.385144	5.395928	0.066280

1.382703	5.398510	0.059479

1.380271	5.399465	0.056982

1.377847	5.392455	0.055097

1.375432	5.374170	0.053345

1.373026	5.353501	0.046728

1.370628	5.344407	0.039854

1.368239	5.345051	0.034649

1.365858	5.350287	0.031416

1.363486	5.352021	0.031070

1.361122	5.333802	0.031047

1.358766	5.306755	0.028833

1.356419	5.286153	0.020849

1.354080	5.282034	0.014566

1.351749	5.285431	0.010692

1.349426	5.290687	0.007035

1.347111	5.296348	0.005947

1.344805	5.293415	0.004218

1.342506	5.291451	0.006455

1.340216	5.286150	0.007330

1.337933	5.275984	0.006428

1.335658	5.263171	0.004786

1.333391	5.253910	0.006953

1.331132	5.238652	0.000316

1.328881	5.228574	0.000000

1.326638	5.225754	0.000000

1.324402	5.213277	0.000000

1.322173	5.203691	0.000000

1.319953	5.202935	0.000000

1.317740	5.209486	0.000000

1.315535	5.204659	0.000000

1.313337	5.201455	0.000000

1.311146	5.189983	0.000000

1.308963	5.181587	0.000000

1.306788	5.173104	0.000000

1.304619	5.177374	0.000000

1.302459	5.175309	0.000000

1.300305	5.177722	0.000000

1.298159	5.179811	0.000000

1.296019	5.178144	0.000000

1.293887	5.181558	0.000000

1.291763	5.172073	0.000000

1.289645	5.160819	0.000000

1.287534	5.164622	0.000000

1.285431	5.152591	0.000000

1.283334	5.139130	0.000000

1.281244	5.148537	0.000000

1.279162	5.135216	0.000000

1.277086	5.143281	0.000000

1.275017	5.136296	0.000000

1.272955	5.139980	0.000000

1.270900	5.135946	0.000000

1.268851	5.135268	0.000000

1.266809	5.138443	0.000000

1.264774	5.147767	0.000000

1.262746	5.155276	0.000000

1.260724	5.158787	0.000000

1.258709	5.166345	0.000000

1.256700	5.165015	0.000000

1.254698	5.152718	0.000000

1.252702	5.145089	0.000000

1.250713	5.146201	0.000000

1.248730	5.148424	0.000000

1.246754	5.157083	0.000000

1.244784	5.167792	0.000000

1.242821	5.174088	0.000000

1.240863	5.185109	0.000000

1.224385	5.075405	0.000000

1.220322	5.071111	0.000000

1.216285	5.062724	0.000000

1.212273	5.068433	0.000000

1.208287	5.063879	0.000000

1.204326	5.062958	0.000000

1.200390	5.061469	0.000000

1.196478	5.058793	0.000000

1.192591	5.054068	0.000000

1.188727	5.053392	0.000000

1.184888	5.054692	0.000000

1.181073	5.056449	0.000000

1.177281	5.052571	0.000000

1.173512	5.052728	0.000000

1.169767	5.047490	0.000000

1.166045	5.044303	0.000000

1.162345	5.041206	0.000000

1.158667	5.043491	0.000000

1.155012	5.037686	0.000000

1.151380	5.038780	0.000000

1.147769	5.040675	0.000000

1.144179	5.037142	0.000000

1.140612	5.038380	0.000000

1.137066	5.033013	0.000000

1.133540	5.028102	0.000000

1.130036	5.023527	0.000000

1.126553	5.013195	0.000000

1.123090	5.018935	0.000000

1.119648	5.023234	0.000000

1.116226	5.020610	0.000000

1.112824	5.011137	0.000926

1.109442	5.020890	0.000000

1.106080	5.013878	0.000000

1.102737	5.008410	0.000000

1.099414	5.000464	0.016160

1.096110	5.004848	0.005657

1.092825	4.999075	0.007874

1.089559	4.995301	0.012315

1.086312	4.999351	0.005270

1.083084	4.998052	0.004549

1.079874	4.988770	0.015609

1.076682	4.992935	0.013112

1.073509	4.991812	0.005625

1.070353	4.987268	0.024756

1.067216	4.981920	0.013343

1.064096	4.976515	0.023154

1.060994	4.976845	0.024852

1.057909	4.983474	0.022199

1.054841	4.980447	0.024470

1.051791	4.979115	0.027456

1.048758	4.973571	0.024259

1.045741	4.982595	0.025136

1.042742	4.973883	0.029518

1.039759	4.969003	0.032471

1.036792	4.968687	0.025326

1.033842	4.963835	0.042203

1.030908	4.960031	0.028998

1.027990	4.972953	0.018507

1.025088	4.968009	0.034877

1.022202	4.957120	0.043559

1.019331	4.956166	0.035414

1.016477	4.949437	0.031330

1.013637	4.952699	0.041151

1.010813	4.959428	0.034149

1.008005	4.955754	0.038712

1.005211	4.956782	0.040015

1.002432	4.948240	0.045634

0.999669	4.958201	0.037426

0.996920	4.927298	0.043052

0.994185	4.948856	0.032524

0.991465	4.935692	0.042734

0.988760	4.939013	0.034134

0.986069	4.935597	0.033770

0.983392	4.938228	0.033633

0.980729	4.947489	0.034011

0.978081	4.937681	0.034461

0.975446	4.947454	0.022701

0.972825	4.925032	0.026105

0.970217	4.934988	0.016697

0.967623	4.928253	0.027527

0.965043	4.936995	0.023589

0.962476	4.951677	0.017285

0.959922	4.925945	0.031652

0.957382	4.970247	0.007112

0.954855	4.951949	0.006413

0.952340	4.916281	0.009714

0.949839	4.922568	0.004172

0.947350	4.909777	0.016730

0.944874	4.914052	0.002855

0.942410	4.922805	0.002152

0.939959	4.909783	0.020426

0.937521	4.906512	0.007752

0.935095	4.905289	0.007245

0.932681	4.919113	0.011324

0.930279	4.909277	0.005094

0.927889	4.933882	0.019507

0.925512	4.883980	0.000000

0.923146	4.883694	0.000000

0.920792	4.879924	0.000000

0.918449	4.899841	0.000000

0.916119	4.879095	0.000000

0.913800	4.873237	0.000000

0.911492	4.862966	0.000000

0.909196	4.873542	0.000000

0.906911	4.865744	0.000000

0.904637	4.872297	0.000000

0.902375	4.856626	0.000000

0.900123	4.852821	0.000000

0.897883	4.843407	0.000000

0.895653	4.824767	0.000000

0.893435	4.839629	0.000000

0.891227	4.822771	0.000000

0.889030	4.838532	0.000000

0.886843	4.809701	0.000000

0.884667	4.822250	0.000000

0.882502	4.826151	0.000000

0.880347	4.805299	0.000000

0.878202	4.808519	0.000000

0.876067	4.803135	0.000000

0.873943	4.812274	0.000000

0.871829	4.797047	0.000000

0.869725	4.775081	0.000000

0.867630	4.804620	0.000000

0.865546	4.781776	0.000000

0.863472	4.770833	0.000000

0.861407	4.735197	0.000000

0.859352	4.764772	0.000000

0.857307	4.799597	0.000000

0.855272	4.784250	0.000000

0.853245	4.729527	0.000000

0.851229	4.790352	0.000000

0.849222	4.790024	0.000000

0.847224	4.713933	0.000000

0.845235	4.736043	0.000000

0.843256	4.749250	0.000000

0.841285	4.753326	0.000000

0.839324	4.704267	0.000000

0.837372	4.734457	0.000000

0.835429	4.653159	0.000000

0.833495	4.699118	0.000000

0.831570	4.739572	0.000000

0.829653	4.748270	0.000000

0.827745	4.701762	0.000000

0.825846	4.651994	0.000000

0.823956	4.698550	0.000000

0.822074	4.698699	0.000000

0.820200	4.695492	0.000000

0.818335	4.684658	0.000000

0.816479	4.708695	0.000000

0.814631	4.726724	0.000000

0.812791	4.666494	0.000000

0.810959	4.674046	0.000000

0.809136	4.669634	0.000000

0.807321	4.684039	0.000000

0.805514	4.682080	0.000000

0.803715	4.659803	0.000000

0.801923	4.704481	0.000000

0.800140	4.698352	0.000000

0.798365	4.712071	0.000000

0.796598	4.638402	0.000000

0.794838	4.667687	0.000000

0.793086	4.631449	0.000000

0.791342	4.690218	0.000000

0.789605	4.680744	0.000000

0.787876	4.639554	0.000000

0.786155	4.771505	0.000000

0.784441	4.629314	0.000000

0.782735	4.673168	0.000000

0.781036	4.706557	0.000000

0.779344	4.623964	0.000000

0.777660	4.572503	0.000000

0.775983	4.743568	0.000000

0.774313	4.640601	0.000000

0.772651	4.670876	0.000000

0.770995	4.686075	0.000000

0.769347	4.568331	0.000000

0.767706	4.649567	0.000000

0.766072	4.597367	0.000000

0.764444	4.772893	0.000000

0.762824	4.749138	0.000000

0.761211	4.721308	0.000000

0.759604	4.635779	0.000000

0.758004	4.657115	0.000000

0.756411	4.630696	0.000000

0.754825	4.576984	0.000000

0.753246	4.754562	0.000000

0.751673	4.617831	0.000000

0.750107	4.683911	0.000000

0.748547	4.848824	0.025729

0.746994	4.686147	0.000000

0.745447	4.564244	0.000000

0.743907	4.696966	0.000000

0.742373	4.607350	0.000000

0.740846	4.666059	0.000000

0.739325	4.667046	0.000000

0.737810	4.627602	0.000000

0.736301	4.880816	0.000000

0.734799	4.657626	0.000000

- ε for FA0.6Cs0.4PbI3 vs. photon energy (eV)

Photon Energy (eV) 	ε1	ε2

5.886830	2.050806	2.737575

5.842581	2.239893	2.783490

5.798990	2.208262	2.892673

5.756044	2.275378	2.836861

5.713730	2.391902	2.795943

5.672031	2.436543	2.796724

5.630938	2.432949	2.721447

5.590435	2.447341	2.693867

5.550508	2.416467	2.602719

5.511149	2.353824	2.542099

5.472343	2.356217	2.537752

5.434079	2.315879	2.458540

5.396346	2.335901	2.386559

5.359134	2.275253	2.335057

5.322429	2.256077	2.406733

5.286224	2.184789	2.342530

5.250508	2.135659	2.325766

5.215272	2.104946	2.303971

5.180504	2.042763	2.335640

5.146196	2.018559	2.363357

5.112340	1.984394	2.354778

5.078925	1.952061	2.406000

5.045945	1.904958	2.421661

5.013389	1.879011	2.437088

4.981251	1.876810	2.510247

4.949521	1.840760	2.537809

4.918193	1.844756	2.585270

4.887259	1.831141	2.656488

4.856710	1.827052	2.668202

4.826542	1.832246	2.714246

4.796745	1.830743	2.745295

4.767314	1.861557	2.780279

4.738242	1.874147	2.794905

4.709521	1.878731	2.801196

4.681147	1.885121	2.818788

4.653112	1.907034	2.835042

4.625410	1.928554	2.834738

4.598037	1.947791	2.866435

4.570985	1.949682	2.877252

4.544249	1.963920	2.877876

4.517825	1.956501	2.865279

4.491704	1.976921	2.866652

4.465886	1.983420	2.871288

4.440361	1.963480	2.853478

4.415126	1.969608	2.868271

4.390176	1.956668	2.876082

4.365508	1.944924	2.868367

4.341113	1.924020	2.868693

4.316990	1.921403	2.883967

4.293134	1.907537	2.873397

4.269539	1.876451	2.881282

4.246203	1.855103	2.891894

4.223120	1.845849	2.901261

4.200286	1.813427	2.906652

4.177698	1.788806	2.930369

4.155352	1.760354	2.956492

4.133243	1.729632	2.998650

4.111368	1.700127	3.001324

4.089723	1.656541	3.026727

4.068305	1.617247	3.064667

4.047110	1.585899	3.098734

4.026134	1.547773	3.133013

4.005375	1.516368	3.169755

3.984829	1.490464	3.220208

3.964492	1.449323	3.269350

3.944361	1.421902	3.319463

3.924434	1.391963	3.380006

3.904708	1.370960	3.441463

3.885178	1.345579	3.538605

3.865843	1.321393	3.605850

3.846699	1.300821	3.666678

3.827744	1.293791	3.753075

3.808975	1.264976	3.844754

3.790389	1.245909	3.911726

3.771983	1.260273	4.000714

3.753756	1.256424	4.081977

3.735703	1.257977	4.183582

3.717823	1.255026	4.274086

3.700114	1.278216	4.345818

3.682572	1.285579	4.436839

3.665196	1.292405	4.559837

3.647983	1.332012	4.644325

3.630931	1.352497	4.730735

3.614038	1.400769	4.835621

3.597301	1.433795	4.914989

3.580719	1.489302	5.035932

3.564288	1.537282	5.107781

3.548008	1.588713	5.211277

3.531876	1.641048	5.311895

3.515889	1.702914	5.406917

3.500047	1.776942	5.510055

3.484347	1.859200	5.588103

3.468787	1.923659	5.687308

3.453366	2.030727	5.758940

3.438081	2.121085	5.857831

3.422931	2.225008	5.924626

3.407914	2.326960	6.008841

3.393028	2.449523	6.089719

3.378271	2.565350	6.148518

3.363643	2.708061	6.205058

3.349140	2.846506	6.289440

3.334762	2.983950	6.301878

3.320507	3.088480	6.364521

3.306374	3.232576	6.376452

3.292360	3.377496	6.407530

3.278465	3.508806	6.424664

3.264686	3.653208	6.402749

3.251023	3.795370	6.396225

3.237473	3.954871	6.372700

3.224037	4.080240	6.356833

3.210711	4.217970	6.290714

3.197495	4.348316	6.245847

3.184388	4.448613	6.165917

3.171387	4.563301	6.123346

3.158493	4.653377	6.041860

3.145703	4.759814	5.987159

3.133016	4.825307	5.925693

3.120431	4.881738	5.852940

3.107947	4.934040	5.803522

3.095562	5.003490	5.710612

3.083276	5.032380	5.634774

3.071087	5.085434	5.581530

3.058994	5.128335	5.518909

3.046996	5.171459	5.469621

3.035092	5.196350	5.422614

3.023281	5.206685	5.360565

3.011561	5.250565	5.317334

2.999932	5.254608	5.260000

2.988392	5.305123	5.221999

2.976941	5.332630	5.176406

2.965577	5.367103	5.135784

2.954300	5.397357	5.090034

2.943108	5.415038	5.036700

2.932001	5.438468	4.989055

2.920978	5.441323	4.949343

2.910037	5.458856	4.907315

2.899178	5.469972	4.874943

2.888400	5.503088	4.829572

2.877702	5.477910	4.800369

2.867082	5.464031	4.754127

2.856541	5.502984	4.722440

2.846077	5.489999	4.692839

2.835690	5.464013	4.687046

2.825378	5.476876	4.672921

2.815142	5.456462	4.646703

2.804979	5.449120	4.648769

2.794889	5.445324	4.631249

2.784872	5.447850	4.629298

2.774927	5.428455	4.635650

2.765052	5.451180	4.659190

2.755248	5.448067	4.666196

2.745512	5.464756	4.672577

2.735846	5.473063	4.686247

2.726248	5.488911	4.717342

2.716716	5.518732	4.741669

2.707252	5.541995	4.736415

2.697853	5.561776	4.774234

2.688519	5.598428	4.781738

2.679250	5.634600	4.811217

2.670044	5.663054	4.835720

2.660902	5.703915	4.859755

2.651822	5.764738	4.873277

2.642804	5.815488	4.883614

2.633847	5.855045	4.883002

2.624951	5.923145	4.898321

2.616115	5.971397	4.896403

2.607338	6.036628	4.917868

2.598620	6.102568	4.914575

2.589961	6.182892	4.917658

2.581358	6.241889	4.903140

2.572814	6.297234	4.890529

2.564325	6.368124	4.866215

2.555892	6.443451	4.855072

2.547515	6.506025	4.831653

2.539193	6.587337	4.794392

2.530925	6.636930	4.769916

2.522711	6.693140	4.723567

2.514550	6.750407	4.682193

2.506442	6.817197	4.653764

2.498386	6.881606	4.608974

2.490382	6.921877	4.542051

2.482429	6.962007	4.488220

2.474527	7.004189	4.457909

2.466675	7.041140	4.404122

2.458873	7.069987	4.356146

2.451120	7.111389	4.285669

2.443417	7.137805	4.239719

2.435761	7.191605	4.191346

2.428154	7.208701	4.142603

2.420594	7.249335	4.093314

2.413081	7.269762	4.032206

2.405614	7.277657	3.979936

2.398194	7.292107	3.921912

2.390820	7.305903	3.864987

2.383491	7.326517	3.819270

2.376207	7.354468	3.783670

2.368967	7.362889	3.735328

2.361772	7.371788	3.687700

2.354620	7.387741	3.647220

2.347511	7.376210	3.600325

2.340446	7.393781	3.546907

2.333423	7.400144	3.504025

2.326442	7.403626	3.456386

2.319503	7.388429	3.424471

2.312605	7.402396	3.388422

2.305749	7.407083	3.346530

2.298933	7.428185	3.320440

2.292157	7.419284	3.272356

2.285422	7.420891	3.238627

2.278726	7.413341	3.197635

2.272069	7.422532	3.145403

2.265451	7.444263	3.140897

2.258872	7.408975	3.101159

2.252331	7.420356	3.047907

2.245827	7.424061	3.040152

2.239362	7.436234	2.994507

2.232934	7.423510	2.956946

2.226542	7.421893	2.934966

2.220187	7.414658	2.890317

2.213869	7.415023	2.859517

2.207587	7.431277	2.844686

2.201340	7.435125	2.814777

2.195129	7.415461	2.790175

2.188952	7.419659	2.752559

2.182811	7.423608	2.731773

2.176704	7.409331	2.703939

2.170631	7.407874	2.670594

2.164593	7.409474	2.641786

2.158587	7.407658	2.617198

2.152616	7.397603	2.590350

2.146677	7.386711	2.556053

2.140771	7.395486	2.534977

2.134898	7.394649	2.522223

2.129057	7.388165	2.483399

2.123248	7.362812	2.452911

2.117471	7.379566	2.435566

2.111725	7.375167	2.407023

2.106011	7.355397	2.386437

2.100327	7.363558	2.371830

2.094674	7.371748	2.350528

2.089052	7.345747	2.321110

2.083460	7.354468	2.301789

2.077898	7.351027	2.275373

2.072366	7.332910	2.240051

2.066863	7.332310	2.230483

2.061389	7.319740	2.207974

2.055945	7.316991	2.193926

2.050529	7.315718	2.181606

2.045143	7.316352	2.153313

2.039784	7.297482	2.141346

2.034454	7.298575	2.126819

2.029151	7.297583	2.087082

2.023876	7.284544	2.078063

2.018629	7.280579	2.072875

2.013409	7.283871	2.063890

2.008216	7.258359	2.024427

2.003050	7.244929	2.003795

1.997911	7.273764	2.009123

1.992798	7.246107	1.980489

1.987711	7.260169	1.966571

1.982651	7.250408	1.932589

1.977616	7.268825	1.938966

1.972607	7.243605	1.900999

1.967623	7.226230	1.898452

1.962664	7.210407	1.849127

1.957731	7.241582	1.843331

1.952823	7.194358	1.821282

1.947939	7.237491	1.817897

1.943080	7.190177	1.796133

1.938245	7.186540	1.796656

1.933434	7.162809	1.768232

1.928647	7.164729	1.761931

1.923884	7.128768	1.757168

1.919145	7.138894	1.739270

1.914429	7.131396	1.717222

1.909737	7.134128	1.730729

1.905067	7.115050	1.710445

1.900420	7.115557	1.699814

1.895796	7.095892	1.697594

1.891195	7.082435	1.688416

1.886616	7.069500	1.690166

1.882060	7.071897	1.677020

1.877525	7.075768	1.661219

1.873013	7.055137	1.664155

1.868522	7.053125	1.652012

1.864053	7.052109	1.641311

1.859605	7.046492	1.629730

1.855179	7.042176	1.628927

1.850774	7.036828	1.620322

1.846390	7.034540	1.619816

1.842026	7.015995	1.620997

1.837684	7.015382	1.613144

1.833362	7.009527	1.613947

1.829061	7.024425	1.597565

1.824779	7.003279	1.596802

1.820518	6.998154	1.596428

1.816277	7.012789	1.580765

1.812056	7.007415	1.585478

1.807855	6.983586	1.585541

1.803673	6.993042	1.574313

1.799510	6.991121	1.572130

1.795367	6.978782	1.571855

1.791243	6.971087	1.567823

1.787138	6.983468	1.560461

1.783052	6.980564	1.559465

1.778985	6.973609	1.556224

1.774937	6.989539	1.556697

1.770907	6.996984	1.552833

1.766895	6.976813	1.555684

1.762902	6.985030	1.551332

1.758927	6.984242	1.550655

1.754970	6.974855	1.544430

1.751030	6.989297	1.549285

1.747109	6.992181	1.548776

1.743205	6.982195	1.549825

1.739319	6.986629	1.548799

1.735450	7.000509	1.548442

1.731599	6.994111	1.546343

1.727765	6.999712	1.546227

1.723948	7.014864	1.553339

1.720148	7.025164	1.546177

1.716365	7.021491	1.552716

1.712598	7.028422	1.547238

1.708848	7.048302	1.546826

1.705115	7.056348	1.549278

1.701398	7.068664	1.546159

1.697697	7.089939	1.539334

1.694013	7.115019	1.536153

1.690345	7.131976	1.529606

1.686693	7.148362	1.521742

1.683056	7.179872	1.509577

1.679436	7.190531	1.485817

1.675831	7.218051	1.471932

1.672242	7.228597	1.447309

1.668668	7.261116	1.422798

1.665109	7.265559	1.393777

1.661566	7.275445	1.360401

1.658038	7.280297	1.323723

1.654526	7.291493	1.288629

1.651028	7.291094	1.258166

1.647545	7.283872	1.220030

1.644077	7.283078	1.184347

1.640624	7.266123	1.152496

1.637185	7.256004	1.119669

1.633761	7.236884	1.094348

1.630351	7.218613	1.063789

1.626956	7.204355	1.039534

1.623574	7.182128	1.012433

1.620207	7.171327	1.000161

1.616855	7.161750	0.983213

1.613516	7.150870	0.970165

1.610191	7.115286	0.945767

1.606880	7.095986	0.932402

1.603582	7.072727	0.915647

1.600299	7.055228	0.905009

1.597028	7.035413	0.891984

1.593772	7.012419	0.883401

1.590528	6.996367	0.868963

1.587298	6.973811	0.859383

1.584082	6.945555	0.838794

1.580878	6.920703	0.818202

1.577688	6.892643	0.810902

1.574510	6.869684	0.804078

1.571346	6.835635	0.779347

1.568194	6.809401	0.771530

1.565055	6.789230	0.768672

1.561929	6.753922	0.749964

1.558815	6.714820	0.741187

1.555714	6.672507	0.728663

1.552625	6.645482	0.721310

1.549549	6.606062	0.715584

1.546485	6.577907	0.699477

1.543433	6.537307	0.689700

1.540394	6.485577	0.691684

1.537367	6.443286	0.678097

1.534351	6.422846	0.659762

1.531348	6.394566	0.644447

1.528356	6.338221	0.636325

1.525376	6.318991	0.620997

1.522408	6.292883	0.600779

1.519452	6.250369	0.586608

1.516507	6.203397	0.567806

1.513574	6.187854	0.545358

1.510652	6.148994	0.516002

1.507742	6.144162	0.502664

1.504843	6.156235	0.494223

1.501955	6.164652	0.486930

1.499079	6.148902	0.474140

1.496213	6.132988	0.459864

1.493359	6.129148	0.450662

1.490516	6.119579	0.438029

1.487683	6.086203	0.416628

1.484862	6.071637	0.400514

1.482051	6.073467	0.391804

1.479252	6.070941	0.386091

1.476462	6.053223	0.372764

1.473684	6.043403	0.360388

1.470916	6.034302	0.343420

1.468159	6.032447	0.339103

1.465412	6.025681	0.329225

1.462675	6.009972	0.316428

1.459949	6.001830	0.311267

1.457233	5.984327	0.297366

1.454528	5.978750	0.291964

1.451832	5.968593	0.276154

1.449147	5.956075	0.263612

1.446472	5.958147	0.265072

1.443806	5.952983	0.255773

1.441151	5.945473	0.247423

1.438506	5.936812	0.233769

1.435870	5.933417	0.222853

1.433244	5.929099	0.219535

1.430628	5.927485	0.211824

1.428022	5.924856	0.203089

1.425425	5.924693	0.200730

1.422838	5.915292	0.187187

1.420260	5.917549	0.191009

1.417692	5.915208	0.184675

1.415133	5.909951	0.173612

1.412584	5.906108	0.165749

1.410044	5.900305	0.160329

1.407513	5.904031	0.158451

1.404991	5.915309	0.154209

1.402479	5.927188	0.153029

1.399975	5.936433	0.151738

1.397481	5.940193	0.152196

1.394996	5.933469	0.144676

1.392519	5.925192	0.142051

1.390052	5.914902	0.137908

1.387594	5.904303	0.133521

1.385144	5.902811	0.126919

1.382703	5.908587	0.124846

1.380271	5.913607	0.122223

1.377847	5.914086	0.116848

1.375432	5.904939	0.115222

1.373026	5.893968	0.111340

1.370628	5.889344	0.111518

1.368239	5.897310	0.108123

1.365858	5.905412	0.106271

1.363486	5.907907	0.105015

1.361122	5.900911	0.100197

1.358766	5.883742	0.100067

1.356419	5.872189	0.094210

1.354080	5.873521	0.090176

1.351749	5.878895	0.091787

1.349426	5.888666	0.087223

1.347111	5.895375	0.086601

1.344805	5.897677	0.086728

1.342506	5.896504	0.085609

1.340216	5.897864	0.086665

1.337933	5.895943	0.082121

1.335658	5.892454	0.083746

1.333391	5.887407	0.086665

1.331132	5.882135	0.077834

1.328881	5.874321	0.078873

1.326638	5.868773	0.079938

1.324402	5.862241	0.072308

1.322173	5.857374	0.076135

1.319953	5.862901	0.064586

1.317740	5.863507	0.067807

1.315535	5.859185	0.066254

1.313337	5.857367	0.062991

1.311146	5.854172	0.068414

1.308963	5.846440	0.070844

1.306788	5.844849	0.065359

1.304619	5.844261	0.062364

1.302459	5.843014	0.064629

1.300305	5.846671	0.061852

1.298159	5.845092	0.055507

1.296019	5.845932	0.054468

1.293887	5.845765	0.054360

1.291763	5.837260	0.059060

1.289645	5.838147	0.054166

1.287534	5.832911	0.057851

1.285431	5.824603	0.045113

1.283334	5.814338	0.055409

1.281244	5.803370	0.059327

1.279162	5.804925	0.054826

1.277086	5.803724	0.048048

1.275017	5.801158	0.048088

1.272955	5.798802	0.052141

1.270900	5.798407	0.043293

1.268851	5.793534	0.040971

1.266809	5.793486	0.042253

1.264774	5.803564	0.042579

1.262746	5.815774	0.036345

1.260724	5.815894	0.037600

1.258709	5.821820	0.040555

1.256700	5.818693	0.039268

1.254698	5.810132	0.039693

1.252702	5.800992	0.034885

1.250713	5.796242	0.035948

1.248730	5.802746	0.032762

1.246754	5.803919	0.035558

1.244784	5.814013	0.032378

1.242821	5.822485	0.029087

1.240863	5.831306	0.029460

1.224385	5.706263	0.022217

1.220322	5.706982	0.020616

1.216285	5.696160	0.017005

1.212273	5.680806	0.026348

1.208287	5.678198	0.019191

1.204326	5.685505	0.015516

1.200390	5.674553	0.018199

1.196478	5.678239	0.008449

1.192591	5.670818	0.009716

1.188727	5.661567	0.004866

1.184888	5.659199	0.005615

1.181073	5.663176	0.000601

1.177281	5.654634	0.001353

1.173512	5.660504	0.000000

1.169767	5.645584	0.000000

1.166045	5.646970	0.000000

1.162345	5.640789	0.000000

1.158667	5.636900	0.000000

1.155012	5.622990	0.000000

1.151380	5.622653	0.000000

1.147769	5.625330	0.000000

1.144179	5.620674	0.000000

1.140612	5.615978	0.000000

1.137066	5.613778	0.000000

1.133540	5.595792	0.000000

1.130036	5.595889	0.000000

1.126553	5.584553	0.000000

1.123090	5.584170	0.000000

1.119648	5.585579	0.000000

1.116226	5.580435	0.000000

1.112824	5.573269	0.000000

1.109442	5.565672	0.000000

1.106080	5.550151	0.000000

1.102737	5.567256	0.000000

1.099414	5.555261	0.000000

1.096110	5.551232	0.000000

1.092825	5.531540	0.000000

1.089559	5.536152	0.000000

1.086312	5.518695	0.000000

1.083084	5.524889	0.000000

1.079874	5.506885	0.000000

1.076682	5.505350	0.000000

1.073509	5.493042	0.000000

1.070353	5.491563	0.000000

1.067216	5.478621	0.000000

1.064096	5.468168	0.000000

1.060994	5.464969	0.000000

1.057909	5.464855	0.000000

1.054841	5.459223	0.000000

1.051791	5.452141	0.000000

1.048758	5.443701	0.000000

1.045741	5.441814	0.000000

1.042742	5.428803	0.000000

1.039759	5.425702	0.000000

1.036792	5.412111	0.000000

1.033842	5.414677	0.000000

1.030908	5.405994	0.000000

1.027990	5.398286	0.000000

1.025088	5.391136	0.000000

1.022202	5.388573	0.000000

1.019331	5.374889	0.000000

1.016477	5.374036	0.000000

1.013637	5.381285	0.000000

1.010813	5.366755	0.000000

1.008005	5.351659	0.000000

1.005211	5.337047	0.000000

1.002432	5.336690	0.000000

0.999669	5.346301	0.000000

0.996920	5.344022	0.000000

0.994185	5.342474	0.000000

0.991465	5.331522	0.000000

0.988760	5.313050	0.000000

0.986069	5.318379	0.000000

0.983392	5.320615	0.000000

0.980729	5.323195	0.000000

0.978081	5.318634	0.000000

0.975446	5.290615	0.000000

0.972825	5.283506	0.000000

0.970217	5.320877	0.000000

0.967623	5.295635	0.000000

0.965043	5.292585	0.000000

0.962476	5.294787	0.000000

0.959922	5.303188	0.000000

0.957382	5.290297	0.000000

0.954855	5.265950	0.000000

0.952340	5.302088	0.000000

0.949839	5.280332	0.000000

0.947350	5.296113	0.000000

0.944874	5.293379	0.000000

0.942410	5.286244	0.000000

0.939959	5.289448	0.000000

0.937521	5.226505	0.000000

0.935095	5.267375	0.000000

0.932681	5.283639	0.000000

0.930279	5.258345	0.000000

0.927889	5.275957	0.000000

0.925512	5.289461	0.000000

0.923146	5.272771	0.000000

0.920792	5.266766	0.000000

0.918449	5.289623	0.000000

0.916119	5.251506	0.000000

0.913800	5.256888	0.000000

0.911492	5.259931	0.000000

0.909196	5.276582	0.000000

0.906911	5.251499	0.000000

0.904637	5.262793	0.000000

0.902375	5.285865	0.000000

0.900123	5.240662	0.000000

0.897883	5.251587	0.000000

0.895653	5.304507	0.000000

0.893435	5.248718	0.000000

0.891227	5.275385	0.000000

0.889030	5.230205	0.000000

0.886843	5.286527	0.000000

0.884667	5.265846	0.000000

0.882502	5.270971	0.000000

0.880347	5.299196	0.000000

0.878202	5.263238	0.000000

0.876067	5.275762	0.000000

0.873943	5.279108	0.000000

0.871829	5.279956	0.000000

0.869725	5.255558	0.000000

0.867630	5.288848	0.000000

0.865546	5.269094	0.000000

0.863472	5.288116	0.000000

0.861407	5.260972	0.000000

0.859352	5.277942	0.000000

0.857307	5.276989	0.000000

0.855272	5.258903	0.000000

0.853245	5.293478	0.000000

0.851229	5.298571	0.000000

0.849222	5.282787	0.000000

0.847224	5.280429	0.000000

0.845235	5.284394	0.000000

0.843256	5.298153	0.000000

0.841285	5.294051	0.000000

0.839324	5.316465	0.000000

0.837372	5.314282	0.000000

0.835429	5.304153	0.000000

0.833495	5.310069	0.000000

0.831570	5.281801	0.000000

0.829653	5.287977	0.000000

0.827745	5.281749	0.000000

0.825846	5.282103	0.000000

0.823956	5.302361	0.000000

0.822074	5.334497	0.000000

0.820200	5.271404	0.000000

0.818335	5.298562	0.000000

0.816479	5.310277	0.000000

0.814631	5.299149	0.000000

0.812791	5.293997	0.000000

0.810959	5.328418	0.000000

0.809136	5.295660	0.000000

0.807321	5.298398	0.000000

0.805514	5.323050	0.000000

0.803715	5.312395	0.000000

0.801923	5.316803	0.000000

0.800140	5.331501	0.000000

0.798365	5.312195	0.000000

0.796598	5.316794	0.000000

0.794838	5.335991	0.000000

0.793086	5.340380	0.000000

0.791342	5.335417	0.000000

0.789605	5.334055	0.000000

0.787876	5.285179	0.000000

0.786155	5.325671	0.000000

0.784441	5.349323	0.000000

0.782735	5.336827	0.000000

0.781036	5.306758	0.000000

0.779344	5.331055	0.000000

0.777660	5.337002	0.000000

0.775983	5.319698	0.000000

0.774313	5.333335	0.000000

0.772651	5.346826	0.000000

0.770995	5.353107	0.000000

0.769347	5.334841	0.000000

0.767706	5.359394	0.000000

0.766072	5.312444	0.000000

0.764444	5.330435	0.000000

0.762824	5.345737	0.000000

0.761211	5.343778	0.000000

0.759604	5.329165	0.000000

0.758004	5.373967	0.000000

0.756411	5.330002	0.000000

0.754825	5.361893	0.000000

0.753246	5.336246	0.000000

0.751673	5.349562	0.000000

0.750107	5.348229	0.000000

0.748547	5.347144	0.000000

0.746994	5.347806	0.000000

0.745447	5.346001	0.000000

0.743907	5.349354	0.000000

0.742373	5.351048	0.000000

0.740846	5.352670	0.000000

0.739325	5.343157	0.000000

0.737810	5.353097	0.000000

0.736301	5.355635	0.000000

0.734799	5.341370	0.000000

References:

[1] Y. Yu, C. Wang, C. R. Grice, N. Shrestha, J. Chen, D. Zhao, W. Liao, A. J. Cimaroli, P. J. Ronald, R.J. Ellingson, and Y. Yan, Improving the performance of formamidinium and cesium lead triiodide perovskite solar cells using lead thiocyanate additives, ChemSusChem 9 (2016) 3288-3297.

[2] Y. Yu, Thin film solar cells with earth abundant elements: Copper Zinc Tin Sulfide to organic-inorganic hybrid perovskite[dissertation]. University of Toledo; 2017.